Supplementary Information25Mg NMR and Computational Modeling Studies of the Solvation Structures and Molecular Dynamics in Magnesium Based Liquid Electrolytes

# Jian Zhi Hu,aǂ* Nav Nidhi Rajput,bǂ Chuan Wanad+ Yuyan Shao,a+

Xuchu Deng,ac Nicholas R. Jaegers,a  Mary Hua, Yingwen Chena, Yongwoo Shin,b Joshua Monk,f Zhong Chenc, Zhaohai Qind, Karl Todd Muellera*, Jun Liua*, and Kristin Perssonbe*

a The Joint Center for Energy Storage Research (JCESR),

Pacific Northwest National Laboratory, Richland, WA 99352, USA
bLawrence Berkeley National Laboratory, Berkeley, CA 94720, USA

cDepartment of Electronic Science, Xiamen University, Xiamen 361005, China

dCollege of Science, China Agricultural University, Beijing 100193, China.

e Department of Materials Science & Engineering, University of California, Berkeley, CA 94720-1760, USA

fNASA Ames Research Center, Moffett Field, CA 94035, USA

ǂ or + These authors have equal contribution to this work.

To whom correspondence should be addressed:

Jian Zhi Hu: Jianzhi.Hu@pnnl.gov; (509) 371-6544.

# Karl.Mueller@pnnl.gov; (509) 371-6550

# Jun Liu: Jun.Liu@pnnl.gov; (509) 375-4443

Kristin Person: kapersson@lbl.gov; (510) 486-7218

30

20

10

0

-10

PPM

0.4M

0.01M

0.005M

0.04M

0.3 ppm

Figure S1. 25Mg NMR spectra of pure Mg(TFSI)2 dissolved in DGM with different concentrations of 0.005, 0.01M, 0.04 and 0.4 M Mg(TFSI)2, illustrating that both the peak center and the linewidth are essentially independent of the Mg(TFSI)2 concentration over a wide range from about 0.005 to about 0.4 M.  1 M MgCl2 in H2O was used as the reference (i.e., 0 ppm).

Figure S2.  25Mg NMR spectra of high salt concentrations of both Mg(BH4)2 and Mg(TFSI)2 dissolved in DGM with different concentrations of Mg(BH4)2 and Mg(TFSI)2.  The linewidths, measured as the full width at the half peak height positions, are approximately:  3.5 ppm for 0.1 M Mg(BH4)2 + 0.1 M Mg(TFSI)2,  4.3 ppm for 0.1 M Mg(BH4)2 + 0.2 M Mg(TFSI)2,  4.5 ppm for 0.1 M Mg(BH4)2 + 0.3 M Mg(TFSI)2,  respectively.

Table S1.  DFT-based 25Mg NMR shielding calculations on the Mg atom for Structure-A showing the similarity of results using both the BLYP-D and the relatively expensive hybrid B3LYPD exchange-correlation functionals.

|  | B3LYPD δcalc ppm (absolute shielding) | **B3LYPD δobs ppm (referenced) | BLYPD δcalc ppm (absolute shielding) | *BYLPD δobs ppm (referenced) |
| --- | --- | --- | --- | --- |
| Mg(H2O)6 | 570.6 | 0 | 565.2 | 0 |
| Mg(BH4)2 DGM | 548.6 | 22.0 | 543.6 | 21.6 |
| Mg(BH4)2 DGM - 1DGM | 543.1 | 27.5 | 539.0 | 26.2 |
| Mg(BH4)2 DGM - 1DGM-2 | 570.7 | -0.1 | 564.6 | 0.6 |
| Mg(BH4)2 DGM -3DGM | 552.0 | 18.6 | 547.1 | 18.1 |

“*” δobs = 565.2 - δcalc ppm

“**”δobs = 570.6 - δcalc ppm

Figure S3. Representative snapshots from MD simulations of a) 0.01 M Mg(BH4)2/DGM b) 0.04 M Mg(TFSI)2/DGM c) 0.4 M Mg(TFSI)2/DGM and d) 0.01 M Mg(BH4)2 + 0.04 M Mg(TFSI)2/DGM solutions.

Figure S4. Geometry optimized structures of the 6-coordinated Mg2+ with and without 2nd solvation shells. (a1) Mg2+(DGM)2, (a2) Mg2+(DGM)2(DGM)2, (a3) Mg2+(DGM)2(DGM)4, (a4) Mg2+(DGM)2(DGM)6, (b1) Mg2+(DGM)3, (b2) Mg2+(DGM)3(DGM)2, (b3) Mg2+(DGM)3(DGM)4, (b4) Mg2+(DGM)3(DGM)6.

Table S2. Calculated 25Mg NMR chemical shifts of the 6-coordinated Mg2+in DGM.

| Label | Structure | 25Mg Chemical shift/ppm |
| --- | --- | --- |
| Figure S4a1 | Mg2+(DGM)2 | -3.6 |
| Figure S4a2 | Mg2+(DGM)2(DGM)2 | -2.2 |
| Figure S4a3 | Mg2+(DGM)2(DGM)4 | 1.1 |
| Figure S4a4 | Mg2+(DGM)2(DGM)6 | 3.2 |
| Figure S4b1 | Mg2+(DGM)3 | -1.7 |
| Figure S4b2 | Mg2+(DGM)3(DGM)2 | -0.8 |
| Figure S4b3 | Mg2+(DGM)3(DGM)4 | 1.7 |
| Figure S4b4 | Mg2+(DGM)3(DGM)6 | 1.8 |

Table S3.  Predicted 25Mg NMR chemical shifts on model solvation structures of possible intermediates in the mixture containing both Mg(BH4)2 and Mg(TFSI)2 dissolved in DGM.

| First solvation shell structure | Solvation structures with 2nd solvation shells | Calculated/predicted 25Mg NMR chemical shifts (ppm) |
| --- | --- | --- |
|  | Mg(BH4)(TFSI)(DGM)-1 | 17.0 |
|  | Mg(BH4)(TFSI)(DGM)-1 + 2 DGMs | 15.4 |
|  | Mg(BH4)(TFSI)(DGM)-1 + 4 DGMs | 15.7 |
|  | Mg(BH4)(TFSI)(DGM)-1 + 6 DGMs | 17.2 |
|  | Mg(BH4)(TFSI)(DGM)-2 | 5.5 |
|  | Mg(BH4)(TFSI)(DGM)-2 + 2 DGMs | 7.4 |
|  | Mg(BH4)(TFSI)(DGM)-2 + 4 DGMs | 4.8 |
|  | Mg(BH4)(TFSI)(DGM)-2 + 6 DGMs | 3.3 |
|  | Mg(BH4)(TFSI)(DGM)-3 | -4.6 |
|  | Mg(BH4)(TFSI)(DGM)-3 + 2 DGMs | -2.8 |
|  | Mg(BH4)(TFSI)(DGM)-3 + 4 DGMs | -4.6 |
|  | Mg(BH4)(TFSI)(DGM)-3 + 6 DGMs | -2.5 |

Table S4: Summary of electrochemical results of electrolyte solutions prepared with two high salt Mg(BH)4 and Mg(TFSI)2 combinations in DGM.

| Mg(BH)4 | Mg(TFSI)2 | Overpotential (V) | Coulombic Efficiency |
| --- | --- | --- | --- |
| 0.1 | 0.1 | 0.19 | 86% |
| 0.1 | 0.2 | 0.19 | 90% |

Optimized geometries Coordinates

Reference Standard

NMR Shielding ADF-GUI atom  Mg(1):         565.19 ppm

Atom            X           Y           Z   (Angstrom)

1.Mg       -0.601196   -0.290594   -0.013291

2.O        -0.403127    1.763767    0.251771

3.O         1.461927   -0.512847    0.121515

4.O        -0.824727   -2.339626   -0.290244

5.O        -2.665571   -0.072523   -0.138345

6.O        -0.747724   -0.562643    2.044678

7.O        -0.442343   -0.012708   -2.069339

8.H        -1.120238    2.425122    0.259987

9.H         0.430240    2.253351    0.384939

10.H         2.107671   -0.480298   -0.608851

11.H         1.969807   -0.679564    0.937730

12.H        -1.668485   -2.813644   -0.412987

13.H        -0.118827   -3.012373   -0.319958

14.H        -3.305840   -0.092273    0.597344

15.H        -3.180577    0.079707   -0.952947

16.H        -0.885535   -1.409712    2.508488

17.H        -0.726709    0.131204    2.730303

18.H        -0.303141    0.837585   -2.526694

19.H        -0.455677   -0.702873   -2.758784

Reference Standard – B3LYPD

NMR Shielding ADF-GUI atom  Mg(1):         570.6 ppm

Atom            X           Y           Z   (Angstrom

1.Mg        0.765800   -1.373314    0.371222

2.H         3.423507   -1.025237    1.026535

3.H         1.268478    1.319728    0.031308

4.H        -1.898743   -1.716813   -0.273024

5.H         0.931507   -1.828707    3.088214

6.H         1.804745   -3.912971    0.641154

7.H         0.755964   -2.454710   -2.165950

8.O         0.703924   -1.619393   -1.681791

9.H         0.604315   -0.920019   -2.342025

10.O         0.974064   -3.419106    0.611688

11.H         0.261893   -4.064536    0.716926

12.O         0.824247   -1.128960    2.429695

13.H         0.769730   -0.294894    2.915637

14.O        -1.292613   -1.569867    0.465787

15.H        -1.832892   -1.535894    1.266952

16.O         0.557500    0.672082    0.130623

17.H        -0.274166    1.164474    0.102902

18.O         2.824003   -1.174956    0.282927

19.H         3.371503   -1.211588   -0.513247

Figure 3a: Mg(BH4)2DGM

NMR Shielding ADF-GUI atom  Mg(24):        543.63 ppm

Atom            X           Y           Z   (Angstrom)

1.O        -0.207990   -0.337490    0.092692

2.C         1.047344    0.012610   -0.541268

3.C         2.129165   -0.365494    0.461240

4.O         1.873614    0.403698    1.657210

5.C         2.760778    0.065747    2.753197

6.C        -1.402627    0.064549   -0.621849

7.C        -2.560962   -0.233586    0.321373

8.O        -2.308276    0.520530    1.525939

9.C        -3.342631    0.374515    2.530775

10.H         1.062837    1.094110   -0.741861

11.H         1.166797   -0.554883   -1.475746

12.H         3.124951   -0.116202    0.064012

13.H         2.075216   -1.440355    0.695858

14.H         2.513504    0.754887    3.565371

15.H         3.804222    0.211603    2.439030

16.H         2.583125   -0.971862    3.068727

17.H        -1.496086   -0.512995   -1.553121

18.H        -1.348401    1.141510   -0.840403

19.H        -2.602692   -1.307133    0.563521

20.H        -3.511866    0.089538   -0.129374

21.H        -4.306113    0.692711    2.107562

22.H        -3.058087    1.033124    3.355438

23.H        -3.379979   -0.667113    2.875384

24.Mg       -0.245982    0.467392    2.105157

25.B        -0.138760    2.869024    2.127923

26.H        -0.142309    2.207051    1.069911

27.H        -0.125707    2.090233    3.120936

28.H         0.885745    3.516982    2.173258

29.H        -1.164064    3.515503    2.187824

30.B        -0.474037   -1.518299    3.388456

31.H        -1.523751   -1.831104    2.847545

32.H        -0.180228   -2.218979    4.329237

33.H         0.434945   -1.553423    2.550660

34.H        -0.587776   -0.350461    3.839753

Figure 3a: Mg(BH4)2DGM – B3LYPD

NMR Shielding ADF-GUI atom  Mg(24):       543.63  ppm

Atom            X           Y           Z   (Angstrom

1.O        -0.208029   -0.337599    0.092614

2.C         1.047840    0.010912   -0.541420

3.C         2.130385   -0.365202    0.461360

4.O         1.873605    0.404053    1.656957

5.C         2.759715    0.065220    2.753194

6.C        -1.402696    0.065231   -0.621594

7.C        -2.561255   -0.232432    0.321559

8.O        -2.307843    0.520954    1.526491

9.C        -3.341924    0.373086    2.531272

10.H         1.063251    1.092098   -0.743997

11.H         1.167329   -0.557972   -1.475043

12.H         3.126079   -0.115704    0.063945

13.H         2.077418   -1.439940    0.696752

14.H         2.512415    0.754119    3.565528

15.H         3.803293    0.210436    2.439862

16.H         2.581538   -0.972485    3.068014

17.H        -1.496645   -0.512350   -1.552816

18.H        -1.347829    1.142096   -0.840217

19.H        -2.603537   -1.306076    0.563185

20.H        -3.511835    0.091423   -0.129272

21.H        -4.305467    0.691345    2.108255

22.H        -3.057603    1.030728    3.356711

23.H        -3.378736   -0.669144    2.874179

24.Mg       -0.245924    0.467656    2.104893

25.B        -0.139770    2.868942    2.127741

26.H        -0.143706    2.207330    1.069558

27.H        -0.126289    2.090494    3.121040

28.H         0.884476    3.517081    2.172160

29.H        -1.165400    3.514849    2.187538

30.B        -0.474426   -1.517605    3.388081

31.H        -1.524148   -1.830047    2.847485

32.H        -0.180748   -2.218322    4.328849

33.H         0.434229   -1.552793    2.550164

34.H        -0.587876   -0.349841    3.839725

Table S3: Mg(BH4)2(DGM)2

NMR Shielding ADF-GUI atom  Mg(24):    538.99   ppm

Atom            X           Y           Z   (Angstrom)

1.O        -0.116279   -0.235364   -0.093897

2.C         1.085621    0.515506   -0.401394

3.C         2.078689    0.151601    0.698848

4.O         1.484210    0.533082    1.962144

5.C         2.222285    0.040937    3.119963

6.C        -1.290409    0.060458   -0.891901

7.C        -2.438827   -0.685911   -0.215534

8.O        -2.485014   -0.243107    1.158163

9.C        -3.495534   -0.910796    1.963172

10.H         0.855170    1.590474   -0.381479

11.H         1.476128    0.219951   -1.386059

12.H         3.025902    0.693769    0.556834

13.H         2.264542   -0.933669    0.698549

14.H         1.674914    0.394908    3.997591

15.H         3.237070    0.461887    3.104601

16.H         2.237581   -1.055849    3.102482

17.H        -1.149314   -0.300215   -1.921184

18.H        -1.471249    1.144529   -0.881167

19.H        -2.263483   -1.773063   -0.241057

20.H        -3.389912   -0.449580   -0.716936

21.H        -4.489614   -0.677225    1.556639

22.H        -3.386882   -0.522178    2.980398

23.H        -3.305458   -1.991691    1.966514

24.Mg       -0.608716    0.190580    1.990362

25.B        -1.104663    2.557707    2.056580

26.H        -0.808170    2.000125    0.990746

27.H        -0.993566    1.749749    3.008729

28.H        -0.307331    3.446176    2.259389

29.H        -2.263750    2.912956    2.006470

30.B        -0.459472   -2.008230    3.056242

31.H        -1.363358   -2.800395    2.872097

32.H         0.328209   -2.352755    3.912998

33.H         0.142269   -1.820071    1.994999

34.H        -0.987129   -0.948756    3.464810

35.O         0.105392    1.637112    5.423753

36.C         0.365230    3.037043    5.202091

37.C         1.697109    3.136902    4.466550

38.O         2.094956    4.515149    4.442886

39.C         3.255039    4.702285    3.633714

40.C        -1.270592    1.409177    5.783170

41.C        -1.454624   -0.089780    6.053109

42.O        -2.745401   -0.487385    5.547821

43.C        -2.933628   -1.903189    5.690147

44.H         0.411187    3.573032    6.165403

45.H        -0.423971    3.475236    4.574280

46.H         1.564509    2.761314    3.439060

47.H         2.463353    2.527747    4.982459

48.H         3.503493    5.769150    3.659960

49.H         3.063692    4.395025    2.588783

50.H         4.111652    4.117829    4.021392

51.H        -1.925017    1.712232    4.950531

52.H        -1.528262    2.015338    6.668612

53.H        -1.397586   -0.316708    7.132993

54.H        -0.661914   -0.649862    5.534579

55.H        -2.180179   -2.455916    5.107166

56.H        -3.936592   -2.132506    5.310955

57.H        -2.870974   -2.203280    6.752134

Table S3: Mg(BH4)2(DGM)2 – B3LYP

NMR Shielding ADF-GUI atom  Mg(24):     543.1  ppm

Atom            X           Y           Z   (Angstrom)

1.O        -0.151933   -0.299242   -0.097133

2.C         1.036725    0.415770   -0.443231

3.C         2.042554    0.085780    0.642280

4.O         1.482608    0.507051    1.885726

5.C         2.232110    0.087542    3.038086

6.C        -1.327754   -0.022684   -0.862572

7.C        -2.455911   -0.743533   -0.149880

8.O        -2.469155   -0.271433    1.193779

9.C        -3.478945   -0.856338    2.026685

10.H         0.826216    1.488540   -0.455986

11.H         1.407087    0.088012   -1.418330

12.H         2.984331    0.612694    0.460707

13.H         2.222168   -0.993770    0.670448

14.H         1.695757    0.464521    3.906732

15.H         3.234299    0.521770    2.997663

16.H         2.271776   -1.002584    3.073076

17.H        -1.214939   -0.399978   -1.882540

18.H        -1.511040    1.054759   -0.871314

19.H        -2.283493   -1.824931   -0.155269

20.H        -3.410519   -0.519047   -0.636122

21.H        -4.465289   -0.592133    1.636963

22.H        -3.338605   -0.447523    3.025910

23.H        -3.344718   -1.939074    2.062571

24.Mg       -0.588121    0.159353    1.970499

25.B        -1.059308    2.507985    2.062467

26.H        -0.784314    1.940944    1.000368

27.H        -0.942767    1.706562    3.011931

28.H        -0.252989    3.386104    2.250103

29.H        -2.210846    2.872439    2.025197

30.B        -0.428120   -2.011715    3.023348

31.H        -1.330341   -2.795306    2.829764

32.H         0.369050   -2.379245    3.853685

33.H         0.154835   -1.797361    1.963695

34.H        -0.944922   -0.967444    3.460323

35.O         0.117663    1.652947    5.441305

36.C         0.377204    3.035735    5.238059

37.C         1.718794    3.164733    4.546613

38.O         2.088645    4.531848    4.569205

39.C         3.227214    4.790034    3.780128

40.C        -1.246129    1.416344    5.766996

41.C        -1.447672   -0.076444    5.993868

42.O        -2.719017   -0.437866    5.465474

43.C        -2.957178   -1.830470    5.569362

44.H         0.397143    3.567230    6.197804

45.H        -0.391210    3.477598    4.597784

46.H         1.621738    2.809168    3.513960

47.H         2.471281    2.553468    5.066277

48.H         3.440739    5.856314    3.850827

49.H         3.048385    4.526216    2.728874

50.H         4.099812    4.225005    4.138708

51.H        -1.885315    1.736697    4.937738

52.H        -1.522293    1.994919    6.657713

53.H        -1.407348   -0.329323    7.061716

54.H        -0.654262   -0.627387    5.480909

55.H        -2.221941   -2.396407    4.988797

56.H        -3.955467   -2.016819    5.172015

57.H        -2.924940   -2.158538    6.616499

Table S1: Mg(BH4)2(DGM)2-2

NMR Shielding ADF-GUI atom  Mg(24):        564.64 ppm

Atom            X           Y           Z   (Angstrom)

1.O         0.324026    0.225345    0.606559

2.C         1.416529    1.170499    0.558188

3.C         2.155673    1.001946    1.878438

4.O         1.200725    1.318156    2.919044

5.C         1.742657    1.194754    4.248818

6.C        -0.592058    0.268139   -0.507713

7.C        -1.692054   -0.724699   -0.163838

8.O        -2.267080   -0.318472    1.106535

9.C        -3.308388   -1.227939    1.532364

10.H         1.009093    2.187953    0.463904

11.H         2.077504    0.932116   -0.288506

12.H         3.009018    1.695330    1.933486

13.H         2.489840   -0.040092    1.998405

14.H         0.918381    1.401174    4.938231

15.H         2.551196    1.926075    4.393773

16.H         2.119512    0.174096    4.410264

17.H        -0.075908   -0.042698   -1.428744

18.H        -0.993807    1.285971   -0.612346

19.H        -1.272325   -1.735734   -0.052429

20.H        -2.474521   -0.712254   -0.937662

21.H        -4.081244   -1.287760    0.752238

22.H        -3.730397   -0.814036    2.449730

23.H        -2.877333   -2.220449    1.727614

24.Mg       -0.721874    0.304587    2.498039

25.B        -1.606909    2.716772    2.260918

26.H        -1.088543    2.271418    1.240688

27.H        -1.247826    2.037256    3.245621

28.H        -1.186765    3.838445    2.476835

29.H        -2.824524    2.658029    2.175671

30.B         0.404423   -2.153651    2.631779

31.H         1.263703   -2.296450    1.781285

32.H         0.442531   -3.005567    3.506678

33.H         0.596424   -1.063088    3.208602

34.H        -0.717319   -2.133072    2.121127

35.O        -0.696179    0.099240    6.709591

36.C         0.396808    0.453012    7.565384

37.C         0.050027    1.803303    8.189925

38.O         1.124922    2.182203    9.056356

39.C         0.855289    3.429540    9.706387

40.C        -0.441472   -1.095928    5.956249

41.C        -1.625135   -1.387197    5.045109

42.O        -1.920315   -0.271988    4.147083

43.C        -2.988033    0.595911    4.640517

44.H         1.333614    0.532740    6.987583

45.H         0.541412   -0.308097    8.351204

46.H        -0.895023    1.718999    8.756249

47.H        -0.092889    2.556062    7.393654

48.H         1.713633    3.651338   10.349321

49.H        -0.059832    3.364658   10.322433

50.H         0.726282    4.242026    8.968912

51.H        -0.302532   -1.962245    6.630063

52.H         0.467426   -0.985141    5.350169

53.H        -2.527466   -1.598045    5.634995

54.H        -1.367960   -2.242555    4.414176

55.H        -3.886929   -0.017043    4.807231

56.H        -3.162912    1.348906    3.869506

57.H        -2.674494    1.069003    5.577397

Table S1: Mg(BH4)2(DGM)2-2 – B3LYP

NMR Shielding ADF-GUI atom  Mg(24):        570.7 ppm

Atom            X           Y           Z   (Angstrom)

1.O         0.370325    0.233324    0.688742

2.C         1.435118    1.180519    0.657003

3.C         2.097125    1.097594    2.014347

4.O         1.087331    1.417652    2.970654

5.C         1.527576    1.363680    4.322086

6.C        -0.470226    0.191411   -0.458692

7.C        -1.563662   -0.797173   -0.125792

8.O        -2.193714   -0.341072    1.076049

9.C        -3.274708   -1.176326    1.480354

10.H         1.026206    2.181058    0.489787

11.H         2.145304    0.917902   -0.132364

12.H         2.919028    1.816886    2.084172

13.H         2.457735    0.080056    2.193187

14.H         0.649866    1.528247    4.945985

15.H         2.270052    2.144668    4.508587

16.H         1.952817    0.380721    4.542450

17.H         0.097665   -0.151934   -1.328617

18.H        -0.889917    1.183886   -0.642695

19.H        -1.136837   -1.788548    0.050628

20.H        -2.300924   -0.834381   -0.933521

21.H        -4.012108   -1.238672    0.675471

22.H        -3.720843   -0.713767    2.355634

23.H        -2.902405   -2.172886    1.733662

24.Mg       -0.761879    0.354652    2.505595

25.B        -1.709886    2.669050    2.215855

26.H        -1.134451    2.190837    1.244763

27.H        -1.325326    2.095522    3.247725

28.H        -1.388951    3.829481    2.342841

29.H        -2.911183    2.504991    2.100054

30.B         0.416260   -2.054449    2.719605

31.H         1.267662   -2.193859    1.868072

32.H         0.480962   -2.883503    3.606467

33.H         0.578340   -0.953093    3.265261

34.H        -0.704701   -2.074021    2.218617

35.O        -0.751247    0.017706    6.726053

36.C         0.369425    0.346498    7.524549

37.C         0.121067    1.715458    8.124954

38.O         1.258461    2.066324    8.887644

39.C         1.117530    3.328571    9.508206

40.C        -0.535908   -1.141138    5.936101

41.C        -1.703254   -1.362217    5.003612

42.O        -1.955461   -0.221840    4.156151

43.C        -3.024506    0.607598    4.652749

44.H         1.282908    0.376507    6.917705

45.H         0.517361   -0.394624    8.320279

46.H        -0.779983    1.689950    8.753139

47.H        -0.049742    2.443509    7.319939

48.H         2.031928    3.520694   10.067754

49.H         0.261978    3.337814   10.196702

50.H         0.973669    4.123087    8.764071

51.H        -0.432849   -2.034371    6.568658

52.H         0.376776   -1.039063    5.346796

53.H        -2.612965   -1.576391    5.568625

54.H        -1.458641   -2.198807    4.354000

55.H        -3.932509    0.001622    4.733235

56.H        -3.165969    1.412048    3.938631

57.H        -2.755124    1.003416    5.631565

Figure 3b: Mg(BH4)2(DGM)4

NMR Shielding ADF-GUI atom  Mg(24):        547.11 ppm

Atom            X           Y           Z   (Angstrom)

1.O        -0.927651   -0.475863   -0.201072

2.C         0.218965   -0.420280   -1.083808

3.C         1.443107   -0.535020   -0.187492

4.O         1.312038    0.502080    0.815747

5.C         2.428569    0.560616    1.741915

6.C        -2.194607   -0.161757   -0.834125

7.C        -3.231441   -0.159468    0.280543

8.O        -2.736268    0.738735    1.294493

9.C        -3.647364    0.906613    2.412805

10.H         0.206996    0.533138   -1.629387

11.H         0.182965   -1.262387   -1.790703

12.H         2.357397   -0.364552   -0.776873

13.H         1.486109   -1.522742    0.291825

14.H         2.247478    1.421755    2.388438

15.H         3.360998    0.703397    1.177386

16.H         2.485572   -0.363902    2.327099

17.H        -2.436539   -0.932116   -1.581935

18.H        -2.114217    0.826737   -1.306753

19.H        -3.343271   -1.165537    0.713484

20.H        -4.195588    0.210770   -0.095561

21.H        -4.598821    1.301259    2.034661

22.H        -3.185348    1.627056    3.091920

23.H        -3.782072   -0.058063    2.920212

24.Mg       -0.661774    0.486879    1.701651

25.B        -0.328650    2.805643    2.105794

26.H        -0.746589    2.353841    1.035958

27.H        -0.230222    1.896514    2.951864

28.H         0.774214    3.274243    1.924645

29.H        -1.146579    3.598466    2.519991

30.B        -0.852635   -1.378480    3.061494

31.H        -1.671292   -1.830960    2.275112

32.H        -0.636938   -2.098387    4.005751

33.H         0.217752   -1.212007    2.449895

34.H        -1.249597   -0.285493    3.484884

35.O        -0.036124    1.785954    5.804296

36.C         1.142613    2.474994    5.364091

37.C         2.221839    1.407481    5.183241

38.O         3.353514    2.018289    4.539214

39.C         4.435786    1.092132    4.402578

40.C        -1.239503    2.550965    5.640768

41.C        -2.396045    1.564836    5.800377

42.O        -3.617528    2.246404    5.456575

43.C        -4.750720    1.392519    5.617157

44.H         1.457779    3.228569    6.107015

45.H         0.965380    2.976121    4.402317

46.H         1.818735    0.590348    4.561165

47.H         2.518995    0.981963    6.157885

48.H         5.234037    1.608560    3.856098

49.H         4.129025    0.189980    3.849231

50.H         4.815897    0.776233    5.391354

51.H        -1.275348    3.000364    4.638459

52.H        -1.300686    3.353766    6.396760

53.H        -2.448546    1.189729    6.837762

54.H        -2.231320    0.706196    5.128820

55.H        -4.663257    0.490646    4.983998

56.H        -5.635596    1.965750    5.318053

57.H        -4.860203    1.067661    6.667694

58.O         1.774816   -3.609599    1.170736

59.C         2.594441   -3.228504    2.284736

60.C         3.878141   -2.640829    1.697119

61.O         4.598989   -1.991100    2.751829

62.C         5.791983   -1.370841    2.263597

63.C         0.509300   -4.187016    1.568119

64.C        -0.465153   -3.904827    0.428657

65.O        -1.673145   -4.643354    0.666382

66.C        -2.703079   -4.245235   -0.234459

67.H         2.823257   -4.098690    2.921792

68.H         2.074235   -2.474422    2.896138

69.H         3.617725   -1.910319    0.912043

70.H         4.494623   -3.432013    1.236094

71.H         6.280169   -0.890963    3.117837

72.H         5.554655   -0.605352    1.501936

73.H         6.473196   -2.115660    1.816296

74.H         0.138056   -3.712809    2.484625

75.H         0.622900   -5.271268    1.729031

76.H        -0.017729   -4.209381   -0.536901

77.H        -0.680052   -2.826136    0.408839

78.H        -2.943855   -3.173136   -0.109978

79.H        -3.590212   -4.845830   -0.004673

80.H        -2.407284   -4.419248   -1.287138

81.O        -1.905724    3.248903   -1.414406

82.C        -3.058279    3.501350   -0.586782

83.C        -4.250078    2.797392   -1.243450

84.O        -5.236951    2.516220   -0.235733

85.C        -6.405336    1.921372   -0.805938

86.C        -0.773791    4.081185   -1.058583

87.C         0.488921    3.274076   -1.342594

88.O         1.626433    4.129885   -1.167009

89.C         2.814320    3.377033   -0.907079

90.H        -3.247716    4.584216   -0.514041

91.H        -2.888640    3.101641    0.422446

92.H        -3.913612    1.854372   -1.709069

93.H        -4.690805    3.422744   -2.039105

94.H        -7.108067    1.733822    0.013050

95.H        -6.160533    0.965031   -1.306579

96.H        -6.873351    2.591671   -1.547886

97.H        -0.796689    4.324592    0.010033

98.H        -0.791936    5.010063   -1.650695

99.H         0.466612    2.869407   -2.373630

100.H         0.530654    2.444670   -0.624907

101.H         2.698444    2.772335    0.007826

102.H         3.630227    4.096217   -0.775112

103.H         3.056872    2.706074   -1.754707

Figure 3b: Mg(BH4)2(DGM)4-B3LYPD

NMR Shielding ADF-GUI atom  Mg(24):        552.0 ppm

1.O        -0.851089   -0.423964   -0.189667

2.C         0.274720   -0.415517   -1.067481

3.C         1.495752   -0.524689   -0.182491

4.O         1.385029    0.518639    0.786747

5.C         2.508384    0.612666    1.670141

6.C        -2.112625   -0.122588   -0.794299

7.C        -3.126249   -0.133826    0.328741

8.O        -2.627465    0.743219    1.331341

9.C        -3.533273    0.957675    2.421858

10.H         0.281621    0.515422   -1.639865

11.H         0.222947   -1.271053   -1.746596

12.H         2.402865   -0.384997   -0.778752

13.H         1.525460   -1.498947    0.311959

14.H         2.317854    1.445271    2.342103

15.H         3.413301    0.808994    1.088442

16.H         2.625688   -0.312826    2.236925

17.H        -2.361149   -0.886368   -1.536951

18.H        -2.054471    0.861963   -1.264314

19.H        -3.227319   -1.140543    0.746669

20.H        -4.092960    0.228609   -0.026416

21.H        -4.459043    1.383812    2.030775

22.H        -3.059442    1.662407    3.100438

23.H        -3.715626    0.010804    2.935115

24.Mg       -0.567140    0.519132    1.690040

25.B        -0.314086    2.851357    2.026700

26.H        -0.608642    2.360458    0.938769

27.H        -0.108333    1.959033    2.865016

28.H         0.713725    3.470920    1.905205

29.H        -1.249740    3.507182    2.417174

30.B        -0.727881   -1.318262    3.060827

31.H        -1.597260   -1.728381    2.313871

32.H        -0.493003   -2.059134    3.976309

33.H         0.307106   -1.177826    2.398250

34.H        -1.060693   -0.221072    3.515168

35.O         0.043131    1.912604    5.862067

36.C         1.211041    2.521478    5.339627

37.C         2.223831    1.409480    5.138119

38.O         3.368095    1.956231    4.500535

39.C         4.414541    1.013389    4.390993

40.C        -1.161137    2.618606    5.615455

41.C        -2.291643    1.625225    5.809438

42.O        -3.509891    2.265867    5.455919

43.C        -4.623074    1.419189    5.630798

44.H         1.606431    3.276775    6.030717

45.H         1.009645    2.999366    4.378081

46.H         1.773393    0.622983    4.519515

47.H         2.494291    0.963398    6.104127

48.H         5.215955    1.482518    3.819244

49.H         4.086240    0.100719    3.881637

50.H         4.797781    0.730994    5.380821

51.H        -1.186665    2.997302    4.590475

52.H        -1.273672    3.464772    6.305974

53.H        -2.326509    1.282988    6.852355

54.H        -2.112427    0.752609    5.170035

55.H        -4.534179    0.511422    5.018647

56.H        -5.509556    1.974022    5.324018

57.H        -4.732805    1.114384    6.679886

58.O         1.684295   -3.620725    1.140728

59.C         2.462102   -3.314425    2.286701

60.C         3.788119   -2.761708    1.797671

61.O         4.445251   -2.162769    2.898670

62.C         5.702535   -1.625454    2.547148

63.C         0.416576   -4.190620    1.460715

64.C        -0.519536   -3.879513    0.310027

65.O        -1.721417   -4.601412    0.514389

66.C        -2.730558   -4.224897   -0.390550

67.H         2.629045   -4.208671    2.898453

68.H         1.949712   -2.568029    2.901721

69.H         3.604877   -2.017112    1.012297

70.H         4.404261   -3.559896    1.363483

71.H         6.130934   -1.183615    3.445327

72.H         5.598433   -0.846610    1.779490

73.H         6.375570   -2.404103    2.167233

74.H         0.013609   -3.748375    2.373522

75.H         0.509896   -5.274872    1.592818

76.H        -0.053252   -4.171928   -0.643042

77.H        -0.716921   -2.802278    0.297553

78.H        -2.976162   -3.157392   -0.289170

79.H        -3.615560   -4.818253   -0.162054

80.H        -2.430656   -4.415461   -1.431505

81.O        -2.004759    3.236561   -1.509307

82.C        -3.110485    3.398430   -0.628758

83.C        -4.292101    2.660308   -1.237105

84.O        -5.229424    2.385269   -0.208427

85.C        -6.390577    1.749495   -0.697661

86.C        -0.905724    4.092675   -1.188227

87.C         0.379500    3.366288   -1.538000

88.O         1.468925    4.257115   -1.361125

89.C         2.560668    3.673317   -0.671132

90.H        -3.356793    4.459093   -0.507411

91.H        -2.872224    2.983750    0.353763

92.H        -3.945979    1.724221   -1.695217

93.H        -4.759752    3.257805   -2.030089

94.H        -7.053576    1.579186    0.149546

95.H        -6.147824    0.784225   -1.165904

96.H        -6.904674    2.371685   -1.440524

97.H        -0.889952    4.317662   -0.121053

98.H        -0.982023    5.028390   -1.752999

99.H         0.344582    3.009773   -2.576897

100.H         0.473488    2.508592   -0.868544

101.H         2.243272    3.289183    0.303792

102.H         3.307390    4.455211   -0.533078

103.H         3.007480    2.853922   -1.254029

Figure 3c: Mg(BH4)2(DGM)6

NMR Shielding ADF-GUI atom  Mg(24):        551.93 ppm

Atom            X           Y           Z   (Angstrom)

1.O        -1.321279   -0.593078   -0.311825

2.C        -0.273498   -0.198161   -1.237264

3.C         1.038479   -0.273094   -0.464681

4.O         0.860215    0.538058    0.719070

5.C         2.073405    0.752686    1.494997

6.C        -2.667025   -0.274225   -0.758286

7.C        -3.603332   -0.587362    0.408554

8.O        -3.051002    0.068803    1.564874

9.C        -3.986853    0.517334    2.591661

10.H        -0.471103    0.823751   -1.585092

11.H        -0.254952   -0.893552   -2.089384

12.H         1.852986    0.139637   -1.079403

13.H         1.271803   -1.309098   -0.182213

14.H         1.782535    1.373802    2.343211

15.H         2.809786    1.291694    0.886114

16.H         2.476200   -0.204761    1.845716

17.H        -2.921760   -0.892948   -1.632649

18.H        -2.701286    0.792014   -1.017038

19.H        -3.662960   -1.670916    0.591222

20.H        -4.601510   -0.182622    0.192006

21.H        -4.881321    0.922033    2.103889

22.H        -3.468380    1.316128    3.127919

23.H        -4.218522   -0.312690    3.267021

24.Mg       -0.967487    0.058675    1.716620

25.B        -1.069426    2.358934    2.278109

26.H        -1.327305    1.959957    1.146509

27.H        -0.941638    1.406498    3.075035

28.H        -0.023342    2.956456    2.258870

29.H        -2.005400    3.014812    2.664067

30.B        -0.389717   -1.950988    2.685026

31.H        -1.091491   -2.218443    1.716715

32.H        -0.174054   -2.942402    3.331880

33.H         0.667091   -1.463275    2.298493

34.H        -0.973454   -1.125598    3.400125

35.O        -0.447781    1.476916    5.705708

36.C         0.836533    1.962049    5.274783

37.C         1.704340    0.726505    5.054345

38.O         3.024824    1.168307    4.683384

39.C         3.961160    0.080928    4.701804

40.C        -1.456921    2.496424    5.694111

41.C        -2.808607    1.795456    5.819951

42.O        -3.829448    2.729879    5.429056

43.C        -5.128510    2.139077    5.514323

44.H         1.285521    2.611064    6.045958

45.H         0.731659    2.538416    4.343723

46.H         1.270440    0.094327    4.260986

47.H         1.753436    0.125762    5.973851

48.H         4.952464    0.509300    4.513695

49.H         3.730678   -0.660379    3.923669

50.H         3.957089   -0.421612    5.682030

51.H        -1.436946    3.036179    4.740527

52.H        -1.295168    3.213157    6.517723

53.H        -2.987577    1.439236    6.849592

54.H        -2.821444    0.920719    5.153072

55.H        -5.200022    1.241451    4.874925

56.H        -5.849647    2.890316    5.173602

57.H        -5.364650    1.844047    6.552599

58.O         1.974320   -3.558756    0.122885

59.C         2.829220   -3.304508    1.247885

60.C         3.908583   -2.330569    0.772057

61.O         4.548449   -1.776710    1.929471

62.C         5.473670   -0.743016    1.576503

63.C         0.811248   -4.345465    0.464882

64.C        -0.279501   -3.944140   -0.524079

65.O        -1.449183   -4.736550   -0.266315

66.C        -2.560048   -4.273503   -1.030987

67.H         3.279212   -4.240790    1.619204

68.H         2.251801   -2.840764    2.060156

69.H         3.432215   -1.527198    0.185823

70.H         4.647722   -2.834298    0.124966

71.H         5.900619   -0.362419    2.508618

72.H         4.959911    0.082506    1.055630

73.H         6.278361   -1.132769    0.928686

74.H         0.473147   -4.109481    1.482096

75.H         1.041138   -5.420727    0.390488

76.H         0.066744   -4.099857   -1.563144

77.H        -0.511970   -2.879924   -0.373379

78.H        -2.800048   -3.223433   -0.781578

79.H        -3.416123   -4.911956   -0.785567

80.H        -2.356295   -4.338019   -2.116838

81.O        -2.745343    3.169775   -1.017214

82.C        -3.838889    3.141931   -0.081946

83.C        -5.006420    2.460959   -0.799892

84.O        -5.957659    2.014450    0.180690

85.C        -7.095751    1.406730   -0.436784

86.C        -1.690337    4.086885   -0.624301

87.C        -0.380029    3.472535   -1.111247

88.O         0.650058    4.470574   -1.094522

89.C         1.913165    3.902795   -1.449205

90.H        -4.118813    4.162472    0.219976

91.H        -3.549439    2.582614    0.818336

92.H        -4.634803    1.597619   -1.380421

93.H        -5.488335    3.155847   -1.508792

94.H        -7.770703    1.088727    0.364943

95.H        -6.798064    0.527290   -1.038616

96.H        -7.617776    2.119961   -1.097912

97.H        -1.679438    4.211671    0.463605

98.H        -1.855578    5.066932   -1.098115

99.H        -0.516670    3.090710   -2.142528

100.H        -0.103922    2.638779   -0.448975

101.H         2.206451    3.110081   -0.739416

102.H         2.655742    4.705804   -1.409179

103.H         1.881374    3.478235   -2.470249

104.O         1.554605    5.129262    2.801876

105.C         2.403800    4.480797    1.850756

106.C         3.591443    3.900080    2.608793

107.O         4.420617    3.199215    1.651276

108.C         5.606393    2.700391    2.274719

109.C         0.366177    5.653979    2.173506

110.C        -0.747757    5.674556    3.215111

111.O        -1.984146    5.924751    2.524318

112.C        -3.108802    5.700816    3.386220

113.H         2.750437    5.191404    1.080366

114.H         1.849091    3.674241    1.347970

115.H         3.249098    3.203261    3.388502

116.H         4.172372    4.709696    3.084070

117.H         6.185242    2.176072    1.505772

118.H         5.359249    2.001588    3.089555

119.H         6.212300    3.525674    2.690209

120.H         0.059441    4.996798    1.353193

121.H         0.566011    6.657280    1.762021

122.H        -0.576325    6.447331    3.986444

123.H        -0.777662    4.687752    3.694581

124.H        -3.125411    4.662962    3.755719

125.H        -4.011045    5.897023    2.794334

126.H        -3.087095    6.388858    4.251476

127.O        -1.383297   -2.026922    7.539874

128.C         0.028070   -1.758964    7.415614

129.C         0.642717   -2.490742    6.216527

130.O         2.076168   -2.387317    6.284819

131.C         2.674572   -2.979285    5.124841

132.C        -2.176062   -1.521230    6.442808

133.C        -2.541580   -2.653238    5.475515

134.O        -3.509193   -2.141050    4.532926

135.C        -3.716896   -3.055263    3.449438

136.H         0.484936   -2.118455    8.345230

137.H         0.197843   -0.675562    7.316573

138.H         0.282999   -2.050681    5.276199

139.H         0.337124   -3.553006    6.236909

140.H         3.758759   -2.860074    5.216394

141.H         2.327594   -2.482321    4.206152

142.H         2.423297   -4.053515    5.057604

143.H        -1.638947   -0.726277    5.910141

144.H        -3.096522   -1.100228    6.870709

145.H        -2.974783   -3.499497    6.037394

146.H        -1.649966   -2.997992    4.935094

147.H        -2.780056   -3.229824    2.898086

148.H        -4.456870   -2.597351    2.780134

149.H        -4.113563   -4.019870    3.814877

Table 2: Mg(BH4)2(DGM)7

NMR Shielding ADF-GUI atom  Mg(24):        550.1 ppm

Atom            X           Y           Z   (Angstrom)

1.O        -0.086073   -0.895398    0.604581

2.C         1.135778   -0.834696   -0.182822

3.C         2.284830   -0.941492    0.800912

4.O         2.030571    0.057237    1.821101

5.C         3.145211    0.255087    2.731356

6.C        -1.295298   -0.602237   -0.152408

7.C        -2.423260   -0.542303    0.863529

8.O        -2.011741    0.388701    1.893051

9.C        -3.011910    0.568394    2.935881

10.H         1.180423    0.127420   -0.712606

11.H         1.162383   -1.661492   -0.897978

12.H         3.227830   -0.728230    0.285432

13.H         2.318747   -1.935943    1.270001

14.H         2.840958    1.029097    3.433988

15.H         4.018325    0.590841    2.154491

16.H         3.370007   -0.671393    3.270304

17.H        -1.477119   -1.391132   -0.888234

18.H        -1.187111    0.363849   -0.659945

19.H        -2.594416   -1.526871    1.324823

20.H        -3.341981   -0.192703    0.378047

21.H        -3.924244    0.987778    2.495906

22.H        -2.599765    1.279431    3.651334

23.H        -3.207716   -0.391934    3.425977

24.Mg        0.020157    0.211377    2.425755

25.B         0.236541    2.607611    2.442158

26.H         0.064600    1.964481    1.403935

27.H         0.506961    1.861577    3.396279

28.H         1.187934    3.331458    2.258639

29.H        -0.781474    3.201058    2.706698

30.B        -0.417803   -1.503392    4.015982

31.H        -1.397194   -1.884505    3.400138

32.H        -0.261293   -2.104329    5.056921

33.H         0.587657   -1.648973    3.314898

34.H        -0.555683   -0.304366    4.297641

35.O        -0.276551   -4.590235    0.426291

36.C        -0.361021   -4.423492   -4.538599

37.H        -0.696673   -6.505652   -4.009019

38.H         0.899434   -5.848095   -3.519746

39.H        -1.374520   -4.004408   -4.401046

40.H        -0.267282   -4.787034   -5.570914

41.C        -0.882325   -5.824576    0.045929

42.H        -0.452850   -1.904514   -3.409733

43.H         1.330706   -1.914902   -3.184219

44.H         0.314674   -3.112344   -2.329091

45.C        -0.178234   -5.618002   -3.595442

46.C         0.436511   -2.540513   -3.258303

47.H         0.775653   -6.318853   -1.249957

48.C        -0.751334   -4.112509    1.696642

49.O         0.641031   -3.411243   -4.391653

50.O        -0.712629   -5.304598   -2.299584

51.C        -0.326183   -6.256775   -1.302813

52.H        -0.720000   -7.260583   -1.551593

53.H        -0.662331   -6.612759    0.791617

54.H        -1.979744   -5.711170   -0.019420

55.H        -0.272571   -3.152581    1.889941

56.H        -0.504178   -4.825352    2.502738

57.H        -1.843942   -3.966634    1.675034

58.O        -4.127151   -0.035816    5.990176

59.C        -3.533023    4.450031    3.516921

60.H        -3.608637    4.872035    5.629066

61.H        -5.091405    4.092000    4.979250

62.H        -2.457593    4.240232    3.428304

63.H        -3.688638    5.530509    3.336541

64.C        -3.351361    0.925015    6.719139

65.H        -3.444292    4.523854    0.838304

66.H        -4.241884    2.930460    0.666198

67.H        -2.634130    3.043966    1.450708

68.C        -3.987659    4.105397    4.926114

69.C        -3.606110    3.539775    1.316734

70.H        -5.034762    2.275227    6.525180

71.C        -3.495110   -1.324510    6.016603

72.O        -4.290112    3.674919    2.571646

73.O        -3.456770    2.821603    5.267075

74.C        -3.930620    2.317932    6.513828

75.H        -3.601048    2.977021    7.341216

76.H        -3.362790    0.674966    7.798598

77.H        -2.308567    0.919089    6.366445

78.H        -4.138288   -2.008009    5.450563

79.H        -3.399493   -1.694399    7.055547

80.H        -2.497547   -1.292495    5.554369

81.O        -1.959331    2.536960   -1.368887

82.C        -3.530169   -2.205243   -2.722766

83.H        -3.905595   -0.830733   -4.339785

84.H        -4.820301   -0.479337   -2.838618

85.H        -2.467926   -2.436642   -2.907591

86.H        -4.142723   -2.943702   -3.274693

87.C        -1.952947    2.358788   -2.787195

88.H        -3.803939   -4.375273   -1.230856

89.H        -3.613695   -3.479345    0.312982

90.H        -2.246333   -3.582630   -0.844945

91.C        -3.843116   -0.808187   -3.234961

92.C        -3.339148   -3.497759   -0.746635

93.H        -4.034087    1.782574   -2.723534

94.C        -0.887219    3.390220   -0.938160

95.O        -3.821590   -2.274906   -1.322055

96.O        -2.807032    0.093548   -2.823608

97.C        -3.096887    1.445752   -3.201522

98.H        -3.222477    1.511415   -4.299406

99.H        -2.080838    3.335112   -3.294087

100.H        -0.991434    1.923228   -3.118088

101.H        -0.932963    3.443232    0.151244

102.H        -0.991997    4.398914   -1.378308

103.H         0.090904    2.973904   -1.234574

104.O         4.173165    2.414091    4.934415

105.C         2.866073   -2.665042    5.526673

106.H         3.149406   -1.675097    7.407226

107.H         4.624044   -1.734851    6.390564

108.H         1.815542   -2.396462    5.339565

109.H         2.897637   -3.621408    6.084569

110.C         3.330570    2.107026    6.061750

111.H         2.819987   -4.729007    3.832106

112.H         3.444503   -3.749858    2.463418

113.H         1.853364   -3.355011    3.196609

114.C         3.528440   -1.585652    6.369406

115.C         2.875169   -3.711858    3.399622

116.H         4.839218    0.690489    6.703656

117.C         3.677654    3.555766    4.219092

118.O         3.567955   -2.816485    4.276897

119.O         3.207301   -0.296938    5.844234

120.C         3.737547    0.764473    6.648067

121.H         3.332402    0.687021    7.675782

122.H         3.445032    2.890091    6.834794

123.H         2.272135    2.080401    5.763320

124.H         4.357523    3.720106    3.374057

125.H         3.666534    4.453033    4.863976

126.H         2.656931    3.382202    3.847670

127.C         4.706109   -2.943923   -1.593008

128.O         3.347907    1.766569   -0.849580

129.H         6.224958   -1.764367   -2.568381

130.H         4.557835   -1.478468   -3.164665

131.H         5.179587   -3.037832   -0.598245

132.H         5.018959   -3.806780   -2.211644

133.C         4.770360    1.788847   -0.975218

134.H         3.030147   -4.998331   -1.343498

135.H         1.696409   -3.975221   -0.711691

136.H         3.207347   -4.151643    0.229435

137.C         5.167049   -1.658465   -2.260993

138.C         2.781318   -4.075204   -0.787189

139.H         4.594435    0.778939   -2.871074

140.C         2.886272    2.702274    0.139015

141.O         3.281290   -2.919722   -1.465046

142.O         5.019360   -0.575023   -1.338538

143.C         5.202592    0.706848   -1.951565

144.H         6.265229    0.855876   -2.221978

145.H         5.111012    2.772744   -1.353515

146.H         5.246465    1.614662    0.007476

147.H         1.807216    2.581599    0.233228

148.H         3.128548    3.739541   -0.159260

149.H         3.337809    2.496488    1.121241

150.C        -0.405448    4.052229    5.971516

151.O        -0.008692    1.674966    6.222160

152.C         0.821490    5.964553    3.814837

153.H         2.065235    6.211590    5.537808

154.H         0.333915    6.573962    5.827839

155.H         1.274934    5.089278    3.327363

156.H         1.312458    6.884897    3.436392

157.C        -0.402257    2.861921    6.922471

158.H        -0.331070    6.934877    1.643705

159.H        -1.885106    6.081657    1.939548

160.H        -0.399680    5.132215    1.631346

161.C         1.038763    5.882828    5.327442

162.C        -0.802988    6.042909    2.097825

163.H        -0.766931    3.751466    4.979530

164.C         0.249672    0.581588    7.105496

165.O        -0.584518    6.020766    3.514236

166.O         0.942601    4.573996    5.896622

167.H        -1.076646    4.833978    6.371811

168.H        -1.411234    2.724781    7.347821

169.H         0.298522    3.065310    7.753900

170.H         0.514138   -0.273669    6.478487

171.H        -0.643023    0.339478    7.711180

172.H         1.083260    0.820927    7.790714

Figure 4a:MgDGM2TFSI-6

NMR Shielding ADF-GUI atom  Mg(24):        564.96 ppm

Atom         X           Y           Z   (Angstrom)

1.O         1.301156   -0.196176    0.675857

2.C         2.742038   -0.147526    0.517352

3.C         3.312077   -0.175933    1.932578

5.C         3.156420    1.062696    4.021673

6.C         0.499135   -0.027075   -0.532433

7.C        -0.915550   -0.404887   -0.113388

8.O        -1.187854    0.251093    1.159982

9.C        -2.507289   -0.081474    1.675483

10.H         3.018478    0.771183   -0.019014

11.H         3.083733   -1.022396   -0.052391

12.H         4.370572    0.119644    1.922149

13.H         3.195989   -1.168083    2.386273

14.H         2.513427    1.790394    4.522420

15.H         4.161788    1.475996    3.866001

16.H         3.205734    0.138074    4.610228

17.H         0.858078   -0.708155   -1.315158

18.H         0.563957    1.012785   -0.878627

19.H        -1.006293   -1.490276    0.033668

20.H        -1.640557   -0.055181   -0.859983

21.H        -3.267317    0.256178    0.958584

22.H        -2.615323    0.447509    2.624036

23.H        -2.582231   -1.162348    1.836872

24.Mg        0.463805    0.745661    2.332201

25.N        -0.013059   -0.884056    3.803780

26.S         0.519072   -2.460336    3.966787

27.S        -0.185206    0.187629    5.016827

28.C        -1.112340   -3.438537    3.664923

29.C        -1.900954   -0.029567    5.871904

30.O        -0.331029    1.438336    4.192776

31.O         0.780433    0.175331    6.095455

32.O         1.343750   -2.717266    2.792618

33.O         0.946624   -2.795084    5.310816

34.F        -2.126534    1.065883    6.623201

35.F        -0.877270   -4.746892    3.857752

36.F        -1.542664   -3.239983    2.383981

37.F        -2.072030   -3.009979    4.520012

38.F        -1.869372   -1.128230    6.641990

39.F        -2.879315   -0.144274    4.936012

40.C        -1.776213    3.270682    0.977073

41.C        -0.579851    3.679751    1.854007

42.O         0.542137    2.740498    1.744356

43.C         1.549716    3.163505    0.774883

44.H        -2.288028    2.418227    1.427458

45.H        -2.484527    4.116553    0.946947

46.H        -0.881590    3.680993    2.908322

47.H        -0.204130    4.675965    1.590288

48.H         1.787803    4.221515    0.945041

49.H         1.181565    3.010420   -0.245595

50.H         2.438280    2.562247    0.975794

51.O        -1.399482    2.854683   -0.342897

52.C        -1.251400    3.940326   -1.285182

53.C        -0.773557    3.344329   -2.607338

54.H        -0.524335    4.682069   -0.913475

55.H        -2.221726    4.445266   -1.427738

56.H        -1.388484    2.468161   -2.850976

57.O         0.592638    2.882415   -2.545176

58.C         1.538132    3.944113   -2.791350

59.H        -0.889839    4.090713   -3.410284

60.H         1.459711    4.740018   -2.030869

61.H         1.371633    4.385385   -3.787049

62.H         2.537828    3.498356   -2.750731

Figure 4b:MgDGM2TFSI-3

NMR Shielding ADF-GUI atom  Mg(24):        570.50 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -0.067472   -0.127589    0.216407

2.C         1.071581    0.229093   -0.618004

3.C         2.225262    0.416260    0.361790

4.O         1.773362    1.331374    1.399639

5.C         2.799870    1.582995    2.404592

6.C        -1.296570   -0.522407   -0.435173

7.C        -2.329737   -0.628003    0.680923

8.O        -2.312031    0.637428    1.407480

9.C        -3.243480    0.632672    2.536493

10.H         0.854516    1.160986   -1.158988

11.H         1.297455   -0.587159   -1.317201

12.H         3.095115    0.848633   -0.153092

13.H         2.502102   -0.539723    0.829489

14.H         2.358210    2.256144    3.142476

15.H         3.665133    2.059004    1.925811

16.H         3.090265    0.641586    2.887441

17.H        -1.168254   -1.493474   -0.932887

18.H        -1.588338    0.235019   -1.174612

19.H        -2.067177   -1.437845    1.376557

20.H        -3.331891   -0.800627    0.264610

21.H        -4.267225    0.516789    2.159552

22.H        -3.124317    1.592102    3.044730

23.H        -2.988868   -0.186395    3.221016

24.Mg       -0.312548    1.265363    1.771470

25.N         0.562538    1.048298    5.194898

26.S        -0.514404    2.186923    4.845450

27.S         0.573313   -0.363620    4.442593

28.C         0.434815    3.678021    5.574601

29.C        -0.561850   -1.493320    5.492369

30.O         1.891757   -0.961245    4.474224

31.O        -0.142169   -0.323671    3.128885

32.O        -0.543889    2.502136    3.374962

33.O        -1.809107    2.119901    5.496707

34.F        -0.553173   -2.737028    4.968246

35.F        -0.308942    4.782184    5.362904

36.F         1.623615    3.817829    4.935820

37.F         0.638058    3.502592    6.884572

38.F        -1.826547   -1.005246    5.462118

39.F        -0.118038   -1.524781    6.755965

40.C        -1.084795    3.018807   -1.849517

41.C        -1.506033    3.331699   -0.402251

42.O        -0.505169    2.958856    0.584778

43.C         0.423467    4.055817    0.901893

44.H        -1.244983    1.952811   -2.092204

45.H        -1.733953    3.607161   -2.522669

46.H        -2.415377    2.770245   -0.158174

47.H        -1.706770    4.404846   -0.291748

48.H        -0.162169    4.930075    1.214226

49.H         1.037697    4.280408    0.025418

50.H         1.037749    3.712863    1.734985

51.O         0.289614    3.344085   -2.025126

52.C         0.709918    3.353004   -3.402862

53.C         2.241807    3.365031   -3.443624

54.H         0.282422    4.231501   -3.912465

55.H         0.353557    2.444715   -3.922448

56.H         2.619625    2.456295   -2.956452

57.O         2.845824    4.455561   -2.749081

58.C         2.659512    5.720902   -3.409794

59.H         2.552470    3.352217   -4.505253

60.H         1.600333    6.026884   -3.411504

61.H         3.024548    5.676261   -4.450519

62.H         3.245304    6.455373   -2.847929

Figure 4c:MgDGM2TFSI5

NMR Shielding ADF-GUI atom  Mg(24):        565.48 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -1.184914   -1.350315    0.261954

2.C         0.122129   -1.855812   -0.175413

3.C         0.837889   -2.343021    1.076050

4.O         0.794148   -1.249132    2.037590

5.C         1.829313   -1.300354    3.068687

6.C        -2.044523   -0.881056   -0.832316

7.C        -3.493157   -1.167908   -0.430773

8.O        -4.319926   -0.370076   -1.268785

9.C        -5.718566   -0.664473   -1.089319

10.H         0.673144   -1.035585   -0.654266

11.H        -0.029983   -2.679812   -0.883056

12.H         1.882841   -2.577320    0.834305

13.H         0.336000   -3.222027    1.506673

14.H         1.731997   -0.391727    3.664127

15.H         2.812000   -1.308960    2.589546

16.H         1.690378   -2.197147    3.686563

17.H        -1.778916   -1.417897   -1.749158

18.H        -1.880407    0.192710   -0.981897

19.H        -3.643448   -0.903258    0.632878

20.H        -3.718761   -2.241791   -0.546539

21.H        -5.930772   -1.718132   -1.330272

22.H        -6.269099   -0.009925   -1.770714

23.H        -6.029627   -0.463544   -0.048430

24.Mg       -0.812329    0.005608    1.810085

25.O        -1.711780   -0.832157    3.555041

26.C        -2.267898   -2.174193    3.264534

27.C        -1.302709   -3.239489    3.792648

28.O        -1.481517   -4.391241    2.967470

29.C        -0.779259   -5.539064    3.486989

30.C        -2.676253    0.120611    4.104010

31.C        -3.542425    0.674107    2.978367

32.O        -2.621829    1.055508    1.925489

33.C        -3.211493    1.952860    0.928069

34.H        -2.373799   -2.286287    2.179526

35.H        -3.254558   -2.254904    3.733432

36.H        -1.514276   -3.472398    4.849919

37.H        -0.270383   -2.864128    3.726737

38.H        -0.971052   -6.365000    2.796214

39.H        -1.148492   -5.799774    4.491328

40.H         0.305157   -5.343070    3.541871

41.H        -2.073574    0.918703    4.550772

42.H        -3.282731   -0.364372    4.878244

43.H        -4.102464    1.553862    3.324272

44.H        -4.247546   -0.077308    2.590790

45.H        -4.004515    1.426627    0.383456

46.H        -2.404218    2.231857    0.252301

47.H        -3.599672    2.841900    1.438622

48.N         1.851526    1.606224    1.909651

49.S         3.396508    2.060546    2.323146

50.S         0.968580    2.374650    0.844602

51.C         4.420263    1.153587    0.967106

52.C         0.034323    3.721317    1.842867

53.O        -0.167889    1.413837    0.567361

54.O         1.533827    3.033872   -0.311291

55.O         3.669635    3.474395    2.150357

56.O         3.693224    1.348102    3.555172

57.F        -0.926735    4.284772    1.071750

58.F         5.727358    1.390267    1.168222

59.F         4.063823    1.566482   -0.265038

60.F         4.199880   -0.195831    1.047083

61.F         0.874732    4.657761    2.284960

62.F        -0.581172    3.120852    2.915878

Figure 4d:MgDGM2TFSI4

NMR Shielding ADF-GUI atom  Mg(24):        571.55 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -1.355800   -1.532931    0.043156

2.C        -0.078683   -2.043499   -0.449524

3.C         0.682207   -2.554959    0.763479

4.O         0.670031   -1.491851    1.751189

5.C         1.635126   -1.676687    2.823684

6.C        -2.257856   -1.080762   -1.022316

7.C        -3.686674   -1.415333   -0.591428

8.O        -4.559492   -0.638597   -1.405225

9.C        -5.943513   -0.950043   -1.157058

10.H         0.465044   -1.228656   -0.944378

11.H        -0.261730   -2.861241   -1.158326

12.H         1.717794   -2.788459    0.479264

13.H         0.202648   -3.447742    1.192287

14.H         1.491342   -0.848806    3.519698

15.H         2.648854   -1.654681    2.404760

16.H         1.451971   -2.635971    3.326787

17.H        -2.000281   -1.597917   -1.953211

18.H        -2.135109   -0.001241   -1.166103

19.H        -3.819557   -1.163666    0.474683

20.H        -3.882982   -2.494907   -0.710820

21.H        -6.151071   -2.010882   -1.370016

22.H        -6.535846   -0.315913   -1.822631

23.H        -6.209164   -0.736004   -0.106299

24.Mg       -0.924849   -0.147300    1.627692

25.O        -2.059783   -1.068793    3.165641

26.C        -2.629145   -2.403423    2.944029

27.C        -1.682801   -3.425940    3.574088

28.O        -2.102838   -4.706409    3.117424

29.C        -1.398607   -5.775757    3.777400

30.C        -2.969290   -0.055668    3.694110

31.C        -3.722964    0.614708    2.547124

32.O        -2.736009    0.934866    1.535450

33.C        -3.235244    1.843348    0.506444

34.H        -2.714996   -2.581371    1.866689

35.H        -3.623127   -2.457994    3.402783

36.H        -1.724214   -3.355367    4.675511

37.H        -0.646279   -3.211201    3.259309

38.H        -1.790160   -6.711979    3.369543

39.H        -1.569985   -5.742623    4.865857

40.H        -0.313958   -5.710385    3.582076

41.H        -2.324789    0.669409    4.199808

42.H        -3.662939   -0.507357    4.413126

43.H        -4.203226    1.537741    2.902924

44.H        -4.489240   -0.046159    2.113104

45.H        -4.023632    1.345850   -0.072461

46.H        -2.385127    2.079703   -0.135306

47.H        -3.609524    2.756267    0.984930

48.N         1.173471    2.821999    1.603836

49.S         0.712041    2.313948    3.042155

50.S         0.839889    2.203729    0.177294

51.C        -0.647035    3.584793    3.481313

52.C         2.469695    1.304444   -0.259879

53.O         0.625000    3.209429   -0.836107

54.O        -0.129948    1.062320    0.191298

55.O        -0.056715    1.030333    3.041353

56.O         1.748397    2.437642    4.039676

57.F         2.278981    0.595483   -1.401252

58.F        -1.223885    3.222379    4.652821

59.F        -1.599205    3.566673    2.507060

60.F        -0.135103    4.814252    3.583819

61.F         2.781865    0.433614    0.739627

62.F         3.468488    2.175264   -0.424409

Figure 5:MgDGM4TFSI

NMR Shielding ADF-GUI atom  Mg(24):        563.97 ppm

Atom            X           Y           Z   (Angstrom)

1.O        -0.110749    0.235455    2.572533

2.C         0.231148    0.562746    3.946820

3.C        -0.736876   -0.224678    4.820074

4.O        -2.075791   -0.030176    4.253868

5.C        -3.138001   -0.566252    5.105353

6.C         0.584347    1.002473    1.538594

7.C         0.160268    0.372966    0.220127

8.O        -1.286416    0.144008    0.267310

9.C        -1.759492   -0.555712   -0.914970

10.H         0.133689    1.647759    4.088083

11.H         1.263323    0.254271    4.151658

12.H        -0.722121    0.149539    5.850717

13.H        -0.506471   -1.293528    4.829729

14.H        -4.078667   -0.359500    4.588769

15.H        -3.103656   -0.060813    6.077911

16.H        -2.997848   -1.642215    5.245602

17.H         1.667888    0.883209    1.660338

18.H         0.295791    2.059012    1.613616

19.H         0.666736   -0.587031    0.078745

20.H         0.380744    1.055795   -0.611049

21.H        -1.474544    0.014329   -1.809678

22.H        -2.846672   -0.609993   -0.832990

23.H        -1.331168   -1.563906   -0.951132

24.Mg       -2.117207   -0.061335    2.159194

25.N        -2.269094   -2.305405    2.015531

26.S        -1.357187   -3.622372    2.466601

27.S        -3.894114   -2.261757    2.037500

28.C        -0.545431   -4.045208    0.773834

29.C        -4.604100   -3.162772    0.480809

30.O        -4.090604   -0.797525    1.758554

31.O        -4.578245   -2.858155    3.165194

32.O        -0.261170   -3.131437    3.290233

33.O        -2.152773   -4.774898    2.843731

34.F        -5.927471   -2.916030    0.427745

35.F         0.189861   -5.164314    0.905049

36.F         0.267737   -3.019260    0.381088

37.F        -1.499000   -4.227593   -0.174635

38.F        -4.375629   -4.480804    0.595112

39.F        -4.012261   -2.690665   -0.646974

40.C        -2.981371    2.687100   -0.172158

41.C        -3.721937    2.477621    1.164846

42.O        -2.879110    1.879276    2.202222

43.C        -2.192974    2.867543    3.032479

44.H        -2.872707    1.731637   -0.688251

45.H        -3.600019    3.351318   -0.801099

46.H        -4.559151    1.785717    1.012593

47.H        -4.113576    3.422086    1.563079

48.H        -2.892564    3.676784    3.278296

49.H        -1.320452    3.262755    2.502813

50.H        -1.907268    2.350500    3.949939

51.O        -1.651857    3.199780   -0.023647

52.C        -1.578163    4.630282    0.155393

53.C        -0.102825    4.997074    0.299307

54.H        -2.141795    4.942064    1.050971

55.H        -2.008961    5.141664   -0.722232

56.H         0.466492    4.518978   -0.508096

57.O         0.465940    4.520606    1.538068

58.C         0.264050    5.441727    2.627348

59.H         0.015740    6.090091    0.217412

60.H        -0.809207    5.596083    2.834227

61.H         0.727650    6.415703    2.402740

62.H         0.744857    5.003177    3.508840

63.O         3.226170   -2.404695    3.848519

64.C         2.682022   -1.965613    5.098907

65.C         3.325238   -2.776857    6.221424

66.O         2.754062   -2.294247    7.443012

67.C         3.276875   -2.971125    8.599147

68.C         2.735324   -1.613450    2.764065

69.C         3.258030   -2.210984    1.462356

70.O         2.824424   -1.341617    0.398693

71.C         3.202595   -1.857397   -0.890297

72.H         1.587595   -2.108019    5.111253

73.H         2.902284   -0.892021    5.256395

74.H         4.420057   -2.635287    6.215172

75.H         3.112262   -3.851815    6.086288

76.H         2.744854   -2.558525    9.461843

77.H         4.361568   -2.794903    8.698796

78.H         3.096774   -4.058050    8.530264

79.H         3.094022   -0.569556    2.862477

80.H         1.634583   -1.611442    2.754579

81.H         2.848063   -3.224703    1.320765

82.H         4.358686   -2.275785    1.481613

83.H         4.298117   -1.953626   -0.968730

84.H         2.845275   -1.143259   -1.641338

85.H         2.741277   -2.844179   -1.065279

86.O         0.844735   -0.824878    9.447651

87.C         1.764247    0.281243    9.427417

88.C         2.550431    0.270786   10.737037

89.O         3.491952    1.346532   10.666765

90.C         4.301376    1.420429   11.851844

91.C         0.112157   -0.924577    8.224458

92.C        -0.491205   -2.325705    8.152561

93.O        -1.227981   -2.421287    6.917236

94.C        -1.752771   -3.746581    6.717799

95.H         1.218843    1.236359    9.324919

96.H         2.457303    0.170819    8.576717

97.H         3.072930   -0.696341   10.853687

98.H         1.868886    0.399473   11.597196

99.H         4.992570    2.259503   11.716207

100.H         4.874902    0.487249   11.994897

101.H         3.676696    1.595395   12.745601

102.H         0.790587   -0.788007    7.367219

103.H        -0.682730   -0.153950    8.186871

104.H        -1.157812   -2.508275    9.012685

105.H         0.325035   -3.064745    8.165052

106.H        -0.937714   -4.488486    6.692122

107.H        -2.274076   -3.752516    5.753464

108.H        -2.458987   -4.013628    7.522072

Figure 5:MgDGM6TFSI

NMR Shielding ADF-GUI atom  Mg(24):        564.00 ppm

Atom            X           Y           Z   (Angstrom)

1.O        -0.211694   -1.992782    2.418302

2.C        -0.863578   -2.638840    3.546725

3.C        -1.665861   -3.794419    2.952616

4.O        -2.350735   -3.275191    1.767320

5.C        -3.326532   -4.224794    1.225622

6.C         0.593584   -0.812227    2.711303

7.C         1.241930   -0.426239    1.392915

8.O         0.183093   -0.416245    0.374655

9.C         0.684342   -0.015657   -0.934013

10.H        -1.497633   -1.911167    4.069716

11.H        -0.099262   -3.027253    4.234245

12.H        -2.418028   -4.161893    3.660634

13.H        -1.003431   -4.612567    2.643164

14.H        -3.772514   -3.735469    0.354372

15.H        -4.082780   -4.421195    1.993636

16.H        -2.807206   -5.142914    0.919821

17.H         1.366841   -1.069109    3.448341

18.H        -0.042757   -0.018989    3.118091

19.H         1.992886   -1.169862    1.088403

20.H         1.678683    0.577376    1.457554

21.H         1.024949    1.023794   -0.878792

22.H        -0.149508   -0.121097   -1.632845

23.H         1.504288   -0.681177   -1.233147

24.Mg       -1.237720   -1.926585    0.634839

25.N        -0.103986   -3.511819   -0.523546

26.S         0.508276   -4.943039    0.073117

27.S        -1.071305   -3.362033   -1.823630

28.C         1.897847   -5.386594   -1.182648

29.C         0.075009   -2.748673   -3.305043

30.O        -1.835772   -2.130654   -1.423110

31.O        -1.799298   -4.507985   -2.326195

32.O         1.174516   -4.584056    1.316588

33.O        -0.451179   -6.034077    0.021330

34.F        -0.412677   -1.574687   -3.777808

35.F         2.427155   -6.578471   -0.848548

36.F         2.861419   -4.435100   -1.164477

37.F         1.363007   -5.456099   -2.431007

38.F         0.064731   -3.668338   -4.279140

39.F         1.343171   -2.555861   -2.868881

40.C        -2.575568    1.661826   -0.178454

41.C        -3.313358    0.324972   -0.072001

42.O        -2.748278   -0.567323    0.933404

43.C        -2.978762   -0.142152    2.319232

44.H        -1.498487    1.482845   -0.275685

45.H        -2.937110    2.180322   -1.086255

46.H        -3.238845   -0.213938   -1.021919

47.H        -4.370460    0.473963    0.180956

48.H        -3.939444    0.374403    2.378283

49.H        -2.173576    0.519762    2.650863

50.H        -3.014936   -1.049828    2.920189

51.O        -2.726431    2.503844    0.973454

52.C        -4.025484    3.124919    1.074227

53.C        -4.016096    4.076583    2.272101

54.H        -4.813403    2.365118    1.199614

55.H        -4.231438    3.694880    0.150114

56.H        -3.074360    4.639634    2.274985

57.O        -4.092193    3.407968    3.541959

58.C        -5.438359    3.008218    3.873228

59.H        -4.854402    4.787797    2.168552

60.H        -5.793574    2.195757    3.221455

61.H        -6.123837    3.870042    3.801703

62.H        -5.413523    2.650671    4.907509

63.O         0.362587    2.956628    2.992233

64.C        -0.854100    3.094699    3.755968

65.C        -0.678404    2.477468    5.129368

66.O        -0.651025    1.043772    5.019619

67.C        -0.460651    0.421691    6.296867

68.C         0.333815    3.791755    1.820086

69.C         1.710443    3.847754    1.183419

70.O         1.998185    2.608810    0.505755

71.C         3.314273    2.620267   -0.076485

72.H        -1.698731    2.633393    3.226314

73.H        -1.088271    4.166144    3.893196

74.H        -1.529742    2.784151    5.763608

75.H         0.256096    2.839039    5.592972

76.H        -0.476598   -0.660872    6.135907

77.H        -1.276679    0.689572    6.989971

78.H         0.501736    0.725907    6.742928

79.H         0.054714    4.822453    2.109218

80.H        -0.418895    3.424709    1.103732

81.H         2.473912    4.036261    1.958045

82.H         1.735418    4.678945    0.456006

83.H         3.408630    3.430954   -0.818864

84.H         3.456929    1.652752   -0.571833

85.H         4.085803    2.754424    0.700283

86.O        -3.429803   -3.710650    7.457301

87.C        -2.817621   -2.839702    6.502079

88.C        -3.498414   -1.477343    6.608754

89.O        -3.145227   -0.729407    5.431102

90.C        -3.739443    0.577441    5.457696

91.C        -2.900173   -5.049767    7.375102

92.C        -3.843393   -5.970336    8.148187

93.O        -3.428138   -7.315771    7.890109

94.C        -4.183586   -8.261466    8.667829

95.H        -2.967415   -3.241265    5.486504

96.H        -1.731192   -2.754543    6.688049

97.H        -3.162474   -0.939771    7.512548

98.H        -4.590152   -1.598906    6.664849

99.H        -3.399170    1.121729    4.574813

100.H        -3.423597    1.129171    6.359529

101.H        -4.838328    0.496663    5.455203

102.H        -1.883386   -5.085926    7.800494

103.H        -2.865360   -5.369359    6.324217

104.H        -4.881649   -5.810449    7.800540

105.H        -3.806284   -5.750645    9.230032

106.H        -4.048439   -8.076558    9.747425

107.H        -3.807187   -9.258155    8.414370

108.H        -5.259915   -8.197527    8.427110

109.O        -8.904647   -1.452746    5.064902

110.C        -8.575726   -0.421048    6.006008

111.C        -8.194849   -1.063677    7.328323

112.O        -6.923695   -1.721265    7.196907

113.C        -6.586092   -2.449432    8.391826

114.C        -9.245325   -0.921607    3.774250

115.C        -9.430374   -2.118527    2.843894

116.O        -9.550223   -1.616294    1.503803

117.C        -9.809481   -2.677407    0.568373

118.H        -9.442703    0.245801    6.162545

119.H        -7.734328    0.185663    5.621829

120.H        -8.970558   -1.794053    7.619199

121.H        -8.140235   -0.284445    8.111100

122.H        -5.609909   -2.915256    8.222890

123.H        -6.530305   -1.771010    9.261751

124.H        -8.431588   -0.279176    3.396298

125.H       -10.169253   -0.320972    3.831733

126.H       -10.332388   -2.688633    3.124778

127.H        -9.884580   -2.220547   -0.424502

128.H       -10.754864   -3.191061    0.811820

129.H        -7.343019   -3.226074    8.598950

130.H        -8.556068   -2.788816    2.927417

131.H        -8.989184   -3.417211    0.577801

132.O        -5.767982   -3.198161    3.430400

133.C        -5.868348   -3.751482    4.761579

134.C        -5.601932   -5.241972    4.713620

135.O        -4.233278   -5.478409    4.330089

136.C        -3.909276   -6.884023    4.374078

137.C        -5.896720   -1.763205    3.463867

138.C        -6.127748   -1.295731    2.028833

139.O        -6.281428    0.143188    2.049485

140.C        -7.028212    0.626512    0.913377

141.H        -6.872837   -3.558885    5.171542

142.H        -5.142513   -3.269312    5.429712

143.H        -6.279398   -5.737233    3.995776

144.H        -5.787761   -5.663854    5.717937

145.H        -2.875058   -6.985026    4.025202

146.H        -3.986526   -7.269511    5.404038

147.H        -4.986667   -1.313656    3.889047

148.H        -6.750309   -1.477969    4.091689

149.H        -7.039337   -1.762947    1.632481

150.H        -7.109147    1.713813    1.028816

151.H        -8.027765    0.170160    0.889596

152.H        -4.577291   -7.457454    3.710198

153.H        -5.275133   -1.573115    1.385431

154.H        -6.505501    0.397341   -0.032408

Figure 5:MgDGM8TFSI

NMR Shielding ADF-GUI atom  Mg(24):        563.62 ppm

Atom            X           Y           Z   (Angstrom)

1.O         0.178333   -1.732501   -0.277911

2.C         1.294814   -1.386921    0.591327

3.C         1.034531   -2.106533    1.904226

4.O        -0.343476   -1.816682    2.300854

5.C        -0.653406   -2.355565    3.628353

6.C         0.119304   -1.011461   -1.549473

7.C        -1.094231   -1.579204   -2.261504

8.O        -2.214878   -1.508950   -1.325480

9.C        -3.435810   -2.055452   -1.909663

10.H         1.343381   -0.302318    0.726741

11.H         2.235614   -1.730241    0.150362

12.H         1.719115   -1.722386    2.670193

13.H         1.138217   -3.194393    1.802763

14.H        -1.702972   -2.130039    3.827077

15.H        -0.011273   -1.870781    4.371875

16.H        -0.476227   -3.434458    3.631512

17.H         1.036943   -1.189498   -2.123585

18.H         0.000027    0.064273   -1.353369

19.H        -0.936019   -2.631517   -2.534129

20.H        -1.328058   -0.970374   -3.140695

21.H        -3.636202   -1.524965   -2.847235

22.H        -4.230188   -1.851856   -1.195500

23.H        -3.327672   -3.134805   -2.070203

24.Mg       -1.666183   -1.606084    0.680165

25.N        -2.412385   -3.724955    0.878828

26.S        -1.703917   -5.217516    1.075083

27.S        -3.678175   -3.250465    1.772791

28.C        -1.136545   -5.485245   -0.747680

29.C        -5.362670   -3.857200    1.024679

30.O        -3.650951   -1.782458    1.479661

31.O        -3.729035   -3.717044    3.144106

32.O        -0.460362   -5.099558    1.826409

33.O        -2.679609   -6.252610    1.375308

34.F        -6.318568   -2.992908    1.452324

35.F        -0.607206   -6.721367   -0.844598

36.F        -0.189579   -4.562837   -1.084312

37.F        -2.177674   -5.366158   -1.603549

38.F        -5.633545   -5.091047    1.476838

39.F        -5.328367   -3.851185   -0.324580

40.C        -2.420429    1.748448   -1.042558

41.C        -2.746544    1.239399    0.364575

42.O        -1.671287    0.419056    0.935878

43.C        -0.646499    1.203629    1.621805

44.H        -2.386586    0.913209   -1.743639

45.H        -3.230308    2.425384   -1.353279

46.H        -3.630996    0.603736    0.316628

47.H        -2.942510    2.051234    1.073074

48.H        -1.143329    1.932175    2.275743

49.H        -0.018201    1.716267    0.890684

50.H        -0.063631    0.512603    2.225400

51.O        -1.141173    2.402158   -1.136937

52.C        -1.143134    3.745961   -0.624252

53.C         0.281041    4.289664   -0.711934

54.H        -1.493907    3.764126    0.422196

55.H        -1.827948    4.375822   -1.216842

56.H         0.675309    4.107977   -1.719409

57.O         1.188977    3.627652    0.195264

58.C         1.086992    4.109452    1.545455

59.H         0.272191    5.376098   -0.518215

60.H         0.057348    4.027101    1.930762

61.H         1.408563    5.162352    1.609297

62.H         1.740837    3.475289    2.154555

63.O         3.938311    0.287085    0.305156

64.C         3.807966    1.550504    0.993345

65.C         3.680493    1.301448    2.485790

66.O         2.348751    0.823439    2.775057

67.C         2.166679    0.570178    4.175969

68.C         3.621442    0.411323   -1.089791

69.C         4.039879   -0.883665   -1.793680

70.O         3.241738   -1.006058   -2.982996

71.C         3.647419   -2.127053   -3.790369

72.H         2.922923    2.094807    0.630036

73.H         4.701007    2.170311    0.801273

74.H         3.860588    2.246543    3.028646

75.H         4.428215    0.560919    2.818449

76.H         1.134161    0.224063    4.308588

77.H         2.324205    1.487103    4.769599

78.H         2.864682   -0.206518    4.533651

79.H         4.143532    1.274759   -1.533462

80.H         2.536377    0.572125   -1.217563

81.H         3.872165   -1.749766   -1.128257

82.H         5.111697   -0.863538   -2.051684

83.H         4.694691   -2.015512   -4.116252

84.H         2.989525   -2.143838   -4.666440

85.H         3.545023   -3.072489   -3.229652

86.O        -4.709419   -2.582579    7.382738

87.C        -4.511526   -2.341018    5.982324

88.C        -3.510798   -1.195289    5.844331

89.O        -3.508113   -0.794387    4.458371

90.C        -2.705314    0.370928    4.241248

91.C        -5.584408   -3.715484    7.578457

92.C        -5.680493   -3.991083    9.075755

93.O        -6.572147   -5.100506    9.236632

94.C        -6.742623   -5.445762   10.618794

95.H        -5.465963   -2.057570    5.502584

96.H        -4.138550   -3.249367    5.491184

97.H        -2.500935   -1.521588    6.144050

98.H        -3.818645   -0.350311    6.481602

99.H        -2.781121    0.603366    3.174972

100.H        -1.647520    0.177062    4.496232

101.H        -3.079836    1.219375    4.834506

102.H        -5.176959   -4.594789    7.059583

103.H        -6.586257   -3.489828    7.172449

104.H        -6.063756   -3.101827    9.609400

105.H        -4.681200   -4.233446    9.482564

106.H        -5.778638   -5.734532   11.075420

107.H        -7.434992   -6.294134   10.654854

108.H        -7.165598   -4.598256   11.188038

109.O        -5.291091   -8.205930   -0.932053

110.C        -5.896701   -8.454539    0.352949

111.C        -5.935353   -9.967603    0.561505

112.O        -6.799764  -10.223916    1.677235

113.C        -6.836626  -11.618526    2.011530

114.C        -5.200216   -6.803701   -1.196182

115.C        -4.741439   -6.627406   -2.641619

116.O        -4.667575   -5.212187   -2.913857

117.C        -4.193261   -4.967379   -4.242701

118.H        -6.927750   -8.057744    0.361337

119.H        -5.326615   -7.964266    1.158074

120.H        -4.920985  -10.356213    0.762293

121.H        -6.323105  -10.460769   -0.348235

122.H        -7.516270  -11.727069    2.864247

123.H        -7.210142  -12.218102    1.161949

124.H        -4.484091   -6.332193   -0.506495

125.H        -6.183904   -6.320058   -1.060207

126.H        -5.457215   -7.109336   -3.329158

127.H        -4.161078   -3.879770   -4.381458

128.H        -4.867377   -5.412500   -4.995324

129.H        -5.831760  -11.982650    2.290530

130.H        -3.752023   -7.094131   -2.786100

131.H        -3.180736   -5.388284   -4.384327

132.O        -5.409810    2.851415    1.413621

133.C        -5.018480    2.972825    2.790590

134.C        -5.702383    1.851409    3.570152

135.O        -5.395942    2.044399    4.955957

136.C        -6.106719    1.099278    5.777362

137.C        -4.920142    3.938103    0.613731

138.C        -5.593134    3.849953   -0.759350

139.O        -4.743595    4.528976   -1.708256

140.C        -5.466933    4.951664   -2.877899

141.H        -5.329156    3.950829    3.194893

142.H        -3.919270    2.894606    2.888584

143.H        -5.344194    0.862203    3.234187

144.H        -6.792727    1.905827    3.402225

145.H        -5.789514    1.270033    6.811649

146.H        -7.196062    1.256321    5.694102

147.H        -3.825477    3.870515    0.489561

148.H        -5.144775    4.902619    1.099178

149.H        -6.587049    4.324490   -0.728695

150.H        -4.743577    5.436880   -3.542798

151.H        -6.260712    5.667499   -2.606980

152.H        -5.865030    0.068170    5.478119

153.H        -5.710141    2.790877   -1.039505

154.H        -5.925515    4.093064   -3.398127

155.O        -3.617080    0.762976   -3.925958

156.C        -4.854295    1.412735   -3.572658

157.C        -5.738405    0.509534   -2.728826

158.O        -5.243210    0.459500   -1.382778

159.C        -6.169882   -0.188122   -0.492226

160.C        -2.817117    1.654670   -4.732359

161.C        -1.570124    0.956166   -5.245431

162.O        -0.585583    0.874584   -4.202972

163.C         0.630429    0.274144   -4.678092

164.H        -5.402217    1.676075   -4.495889

165.H        -4.642393    2.342139   -3.020030

166.H        -5.785473   -0.506345   -3.159361

167.H        -6.760372    0.929628   -2.732828

168.H        -5.715083   -0.184777    0.503078

169.H        -7.126758    0.358438   -0.462842

170.H        -2.530210    2.539796   -4.138902

171.H        -3.411683    1.991070   -5.600814

172.H        -1.164462    1.537596   -6.093116

173.H         1.350657    0.283726   -3.855445

174.H         1.041424    0.838119   -5.532876

175.H        -6.359456   -1.227862   -0.808166

176.H        -1.826679   -0.054149   -5.615422

177.H         0.454434   -0.769547   -4.999905

178.O        -3.280527   -5.622595    5.908747

179.C        -1.975787   -5.062540    5.714878

180.C        -1.664713   -4.186355    6.930463

181.O        -0.660380   -3.222504    6.537423

182.C        -0.263600   -2.412994    7.655312

183.H        -3.303051   -7.529833    5.033174

184.H        -5.622344   -6.760614    5.754211

185.H        -1.973078   -4.442664    4.805607

186.H        -1.220393   -5.858012    5.594909

187.H        -1.287980   -4.795241    7.769938

188.H         0.488321   -1.702223    7.291181

189.H         0.175970   -3.033094    8.455328

190.H        -2.577229   -3.665535    7.260157

191.H        -1.126349   -1.861097    8.068055

192.C        -3.669767   -6.509180    4.836235

193.C        -5.195223   -6.489215    4.771587

194.O        -5.604545   -7.423785    3.768702

195.C        -7.035974   -7.478234    3.658188

196.H        -3.257501   -6.164190    3.878559

197.H        -5.539436   -5.469928    4.517128

198.H        -7.269251   -8.257833    2.927947

199.H        -7.492563   -7.731632    4.631554

200.H        -7.437552   -6.503216    3.324475

Figure S4a1: Mg2+(DGM)2

NMR Shielding ADF-GUI atom  Mg(24):        568.79 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -1.404840    0.607696    2.682633

2.C        -0.297449    0.131867    1.856939

3.C         0.946572    0.257631    2.724050

4.O         0.948522    1.616240    3.256741

5.C         2.168353    1.937144    3.986984

6.C        -2.702015    0.672361    2.015074

7.C        -3.673988    1.210821    3.054955

8.O        -3.056572    2.395010    3.648413

9.C        -3.944089    3.068341    4.593460

10.H        -0.225154    0.761260    0.958579

11.H        -0.469261   -0.911832    1.565422

12.H         1.849062    0.093206    2.120404

13.H         0.927560   -0.457825    3.559290

14.H         3.034850    1.821633    3.324927

15.H         2.267776    1.282241    4.863004

16.H         2.079298    2.982312    4.297277

17.H        -3.004627   -0.328410    1.682379

18.H        -2.623303    1.343788    1.148592

19.H        -4.625918    1.485873    2.581435

20.H        -3.858551    0.471346    3.847382

21.H        -3.384662    3.916081    4.994890

22.H        -4.224313    2.377496    5.400715

23.H        -4.843426    3.412785    4.068797

24.Mg       -0.957006    2.317412    3.825003

25.H        -1.888797    5.488581    3.218847

26.H        -2.132042    4.178620    1.030332

27.H        -0.864011    2.933391    0.736580

28.H        -0.465049    4.669179    0.557122

29.H         0.876765    3.431518    6.346483

30.H        -0.400754    4.391609    7.166486

31.H        -1.982494    2.506757    7.081933

32.H        -0.436954    1.863015    7.728110

33.C        -0.817507    5.249420    3.148450

34.H        -0.870927   -0.390432    6.825948

35.H        -1.375967   -0.499274    5.101226

36.H        -2.485552    0.213001    6.324075

37.O        -0.658463    3.944181    2.515688

38.C        -0.206533    3.589487    6.443422

39.C        -0.924782    2.311914    6.852632

40.C        -1.436978    0.089770    6.018915

41.H         0.910026    5.027311    4.456610

42.O        -0.849966    1.393297    5.718371

43.O        -0.751958    3.949371    5.137389

44.C        -1.063416    3.939650    1.115887

45.C        -0.180401    5.146948    4.526592

46.H        -0.419678    6.027826    5.135300

47.H        -0.308216    6.016991    2.550658

Figure S4a2: Mg2+(DGM)2(DGM)2

NMR Shielding ADF-GUI atom  Mg(24):        567.36 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -0.977867    0.847065    3.096961

2.C         0.149779    0.497164    2.247656

3.C         1.277694    0.119899    3.197939

4.O         1.414797    1.212265    4.145683

5.C         2.558463    1.039277    5.045728

6.C        -2.161069    1.365858    2.405877

7.C        -3.150175    1.749133    3.491089

8.O        -2.395071    2.533946    4.474644

9.C        -3.232384    3.363382    5.334192

10.H         0.423127    1.368431    1.633531

11.H        -0.114942   -0.345863    1.595976

12.H         2.217502   -0.008894    2.643671

13.H         1.043427   -0.808681    3.740541

14.H         2.661908    1.959153    5.621430

15.H         3.462998    0.891849    4.443721

16.H         2.388316    0.182458    5.707814

17.H        -2.575231    0.589361    1.749835

18.H        -1.868223    2.240666    1.810401

19.H        -3.574926    0.874052    3.996115

20.H        -3.958860    2.360504    3.078774

21.H        -3.714191    4.131975    4.721314

22.H        -2.559622    3.810389    6.071250

23.H        -3.994483    2.743037    5.818040

24.Mg       -0.416459    2.023201    4.766388

25.H        -7.323317    1.331874    4.005613

26.H        -7.717990    1.764114    5.698439

27.C        -5.060153    4.897864    1.686039

28.H        -6.699144   -0.286779    6.476587

29.H        -4.996902   -0.592160    6.007703

30.H        -6.303834   -0.730882    4.784984

31.O        -3.672894    4.508385    1.831388

32.C        -6.707673    3.309611    4.611337

33.C        -6.949024    1.840077    4.910488

34.H        -5.223504    5.388772    3.789715

35.C        -3.005739    4.560712    0.559308

36.O        -5.730278    1.209264    5.359332

37.O        -5.921044    3.447408    3.414547

38.C        -5.778434    4.820514    3.020675

39.H        -6.771911    5.286940    2.906914

40.H        -5.116251    5.933948    1.311457

41.H        -5.557871    4.233733    0.959636

42.H        -1.963361    4.266383    0.723676

43.H        -3.030185    5.578839    0.137753

44.H        -3.471782    3.868966   -0.162128

45.C         0.817700    4.188611    6.409607

46.H         0.746836    4.829510    7.298181

47.H         0.969259    5.729185    4.899171

48.H        -0.718133    5.321558    5.366193

49.H        -0.208598    3.737728    2.109010

50.H         0.228878    5.399595    2.599017

51.H        -1.401624    4.733242    3.006463

52.H         0.189934    2.654165    8.618645

53.H         1.291266    1.740659    7.528290

54.H        -1.773563    1.402496    7.811658

55.H        -0.514979    0.205467    8.279040

56.C         0.289193    4.917089    5.184809

57.H        -1.631017   -1.345804    6.674465

58.H        -1.719444   -0.808986    4.960177

59.H        -2.789400   -0.054771    6.190616

60.O         0.217414    3.942138    4.102825

61.C         0.271548    2.124621    7.660207

62.C        -0.767882    1.017122    7.585040

63.C        -1.799320   -0.494286    6.002908

64.H         1.850334    3.850767    6.265861

65.H        -7.686162    3.799918    4.473115

66.H        -6.197208    3.795201    5.461875

67.C        -5.954360   -0.175973    5.671732

68.C         3.325022    5.050188    3.560982

69.O         2.952193    0.421319    8.238595

70.O         4.091788    3.029137    7.306928

71.C         5.096346    3.671926    6.495527

72.H         5.851944    4.146676    7.145102

73.H         5.312201    5.275558    5.113070

74.H         3.926950    5.478428    6.226091

75.H         2.611411    4.545215    2.902553

76.H         4.241277    5.299504    3.002194

77.H         2.883472    5.993662    3.930594

78.H         5.419529    2.611776    8.864058

79.H         5.297185    1.342521    7.610270

80.H         3.004587    2.083735    9.515741

81.H         4.229312    0.821585    9.844454

82.C         4.485362    4.745857    5.615732

83.H         2.767921   -1.025477    9.750752

84.H         1.621440   -1.127848    8.377456

85.H         1.410856    0.135211    9.642777

86.O         3.610508    4.148185    4.639159

87.C         4.721686    2.080646    8.194383

88.C         3.694025    1.359974    9.044510

89.C         2.145614   -0.443099    9.053329

90.H         5.603463    2.921198    5.865895

91.C        -0.335438    4.501859    2.881679

92.O        -0.763718    0.507005    6.215153

93.O        -0.063809    3.032599    6.567410

Figure S4a3: Mg2+(DGM)2(DGM)4

NMR Shielding ADF-GUI atom  Mg(24):        564.06 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -2.549354    0.700740    3.233611

2.C        -1.701093   -0.071933    2.335398

3.C        -0.529709   -0.530733    3.199730

4.O         0.055035    0.625334    3.868761

5.C         1.280830    1.123122    3.206652

6.C        -3.671437    1.393786    2.599760

7.C        -4.341383    2.202164    3.695726

8.O        -3.290025    2.988471    4.335507

9.C        -3.803041    3.830180    5.415232

10.H        -1.362021    0.565362    1.509871

11.H        -2.264005   -0.930848    1.943723

12.H         0.224701   -1.043435    2.591693

13.H        -0.883524   -1.206830    3.987381

14.H         1.538286    2.071211    3.681509

15.H         1.093119    1.294731    2.142123

16.H         2.071228    0.375654    3.350987

17.H        -4.369365    0.658204    2.178335

18.H        -3.275486    2.034849    1.800105

19.H        -4.814401    1.560243    4.450265

20.H        -5.097320    2.880449    3.287582

21.H        -4.616142    4.444210    5.021363

22.H        -2.966386    4.458997    5.728687

23.H        -4.166861    3.200394    6.234767

24.Mg       -1.424994    2.035544    4.434103

25.H        -7.822363    1.315947    5.288312

26.H        -8.167298    1.761738    6.988252

27.C        -6.621395    5.223275    2.661924

28.H        -6.560131    0.148682    7.786884

29.H        -4.885115    0.275069    7.157906

30.H        -6.202407   -0.338709    6.100754

31.O        -5.199746    5.295808    2.886058

32.C        -7.708932    3.429282    5.723146

33.C        -7.519563    1.975693    6.120410

34.H        -6.969525    5.752984    4.726930

35.C        -4.465268    5.388602    1.660266

36.O        -6.142259    1.731076    6.467835

37.O        -7.079561    3.678769    4.454389

38.C        -7.330260    5.014489    3.989028

39.H        -8.413836    5.170408    3.847146

40.H        -6.976435    6.159938    2.199232

41.H        -6.855933    4.386776    1.979703

42.H        -3.409346    5.530043    1.905199

43.H        -4.806463    6.245200    1.054960

44.H        -4.585352    4.469518    1.057483

45.O         2.067385    4.928522    7.548304

46.O         0.849443    7.386260    6.316338

47.C         0.527369    8.195232    5.175655

48.H         1.101840    9.138237    5.209515

49.H        -1.127686    9.336867    4.429511

50.H        -1.280451    8.875251    6.153047

51.H        -3.595076    6.723806    4.280377

52.H        -3.271552    8.441770    3.886419

53.H        -3.545263    7.955354    5.589302

54.H         2.863094    7.933608    6.265538

55.H         2.466099    6.406891    5.421458

56.H         2.218557    6.809725    8.458393

57.H         3.703132    6.221240    7.648037

58.C        -0.956075    8.524973    5.159120

59.H         3.592785    4.123131    8.751328

60.H         2.079045    3.175676    8.613559

61.H         2.124785    4.653207    9.633452

62.O        -1.704326    7.358979    4.768775

63.C        -3.107613    7.640620    4.627556

64.C         2.239217    7.022932    6.308947

65.C         2.602060    6.269067    7.577001

66.C         2.493083    4.186579    8.705057

67.H         0.797718    7.663597    4.247410

68.C         3.640949    4.039962    4.554160

69.O         0.252333    0.850414   -0.241482

70.O         2.141755    2.989482    0.696957

71.C         2.582348    4.322835    0.995374

72.H         3.156769    4.723534    0.141738

73.H         4.080529    5.251797    2.224840

74.H         4.211490    3.472022    2.113076

75.H         3.029025    4.004030    5.461287

76.H         4.335724    4.895167    4.623341

77.H         4.235385    3.115508    4.461037

78.H         2.203682    3.361623   -1.356677

79.H         0.577037    3.454739   -0.627222

80.H         2.263439    0.892665   -0.818700

81.H         1.091028    1.409742   -2.070602

82.C         3.500839    4.311180    2.206559

83.H        -0.097295   -0.635444   -1.687711

84.H        -0.740979   -0.937214   -0.046166

85.H         1.017966   -1.103663   -0.366936

86.O         2.752668    4.190926    3.431911

87.C         1.531009    2.909729   -0.605718

88.C         1.332152    1.456833   -0.994886

89.C         0.106490   -0.532265   -0.609477

90.H         1.725115    4.995848    1.159546

91.C        -0.919952    3.537667    1.738401

92.O        -1.820622    1.173830    6.347256

93.O        -0.506526    3.319548    5.717186

94.C        -0.099995    4.632166    5.191644

95.H        -0.443332    5.433289    5.849158

96.H        -0.200976    5.513054    3.224140

97.H        -1.791555    5.033968    3.865083

98.H        -0.682796    2.567218    1.301163

99.H        -0.307153    4.309648    1.274657

100.H        -1.973037    3.801780    1.593696

101.H        -1.710372    3.737933    7.369521

102.H         0.046982    3.617149    7.711846

103.H        -1.369393    1.515542    8.371335

104.H         0.039816    1.191557    7.300687

105.C        -0.732328    4.761099    3.812119

106.H        -2.597073   -0.406153    7.480852

107.H        -1.161189   -0.817048    6.480772

108.H        -2.756215   -0.528840    5.695670

109.O        -0.615496    3.461001    3.156930

110.C        -0.782436    3.200000    7.130782

111.C        -0.931003    1.703261    7.381380

112.C        -2.096549   -0.239851    6.517956

113.H         0.988690    4.636678    5.135636

114.C        -2.423798    3.061552   -1.362679

115.O         1.341436    7.614218    0.298940

116.O        -1.396701    6.535234    0.817959

117.C        -1.386912    6.556826   -0.631771

118.H        -1.795793    7.518334   -0.985644

119.H        -2.425386    5.597944   -2.246450

120.H        -3.246384    5.448298   -0.663510

121.H        -1.836092    2.157178   -1.166009

122.H        -2.672853    3.120387   -2.435427

123.H        -3.368388    3.026925   -0.787296

124.H        -1.251217    7.773638    2.425798

125.H        -1.103767    8.606982    0.843155

126.H         1.002701    6.795404    2.180031

127.H         1.006243    8.579872    2.122997

128.C        -2.264062    5.436902   -1.166131

129.H         3.026421    8.733687    0.857587

130.H         3.186178    7.679317   -0.586285

131.H         3.186720    6.958324    1.058639

132.O        -1.618014    4.170001   -0.952166

133.C        -0.821447    7.710042    1.418178

134.C         0.698663    7.668814    1.573376

135.C         2.765786    7.754871    0.421100

136.H        -0.360398    6.456035   -1.008947

137.C        -5.945325    0.378300    6.900889

138.H        -8.791920    3.631742    5.652396

139.H        -7.281976    4.091745    6.496280

Figure S4a4: Mg2+(DGM)2(DGM)6

NMR Shielding ADF-GUI atom  Mg(24):        561.98 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -2.475646    1.130487    2.685288

2.C        -1.239746    0.585747    2.105675

3.C        -0.278901    0.365655    3.265673

4.O        -0.361578    1.555217    4.119546

5.C         0.701744    1.632571    5.092071

6.C        -3.489208    1.560056    1.742953

7.C        -4.622367    2.120627    2.594223

8.O        -4.036939    3.131347    3.455623

9.C        -4.974886    3.608195    4.482865

10.H        -0.845248    1.312492    1.384464

11.H        -1.455223   -0.363556    1.606256

12.H         0.739334    0.269885    2.885021

13.H        -0.554680   -0.515190    3.855652

14.H         0.524528    2.533496    5.684653

15.H         1.658208    1.705306    4.569001

16.H         0.690524    0.733493    5.723291

17.H        -3.837297    0.708188    1.142429

18.H        -3.067683    2.328439    1.077633

19.H        -5.065963    1.325386    3.212575

20.H        -5.406972    2.576341    1.976540

21.H        -5.932586    3.852131    4.018314

22.H        -4.512493    4.493265    4.923047

23.H        -5.112390    2.825248    5.234271

24.Mg       -2.075020    2.642165    4.096822

25.H        -7.049401    1.633552    6.386489

26.H        -8.157539    2.210716    7.671089

27.C        -8.391403    3.389047    2.039825

28.H        -6.286276    3.179871    8.869902

29.H        -5.258665    4.354889    7.978042

30.H        -5.164130    2.611395    7.592614

31.O        -7.340412    4.370941    2.090763

32.C        -8.743216    2.778574    5.682588

33.C        -7.671586    2.485973    6.718127

34.H        -9.430979    4.313497    3.685069

35.C        -6.798620    4.643396    0.796090

36.O        -6.851903    3.650315    6.906024

37.O        -8.153048    2.811502    4.371867

38.C        -9.075570    3.310418    3.392284

39.H        -9.951145    2.641627    3.308422

40.H        -9.141398    3.674319    1.282014

41.H        -7.972545    2.404402    1.762246

42.H        -6.000774    5.378566    0.930609

43.H        -7.567648    5.048135    0.117015

44.H        -6.373456    3.733146    0.337109

45.O         0.910071    3.844878    7.914975

46.O        -0.034706    6.702091    7.498052

47.C         0.082899    8.106509    7.178156

48.H         0.120850    8.683807    8.118704

49.H        -1.194435    9.676263    6.480403

50.H        -2.034085    8.111293    6.718865

51.H        -1.776251    8.529757    3.130481

52.H        -1.992040    9.923889    4.246524

53.H        -2.949172    8.420746    4.482952

54.H         1.264873    6.969571    9.108038

55.H         1.997334    6.223354    7.658208

56.H        -0.173399    4.881392    9.377202

57.H         1.585801    4.733294    9.679134

58.C        -1.105084    8.582198    6.354824

59.H         1.866116    2.508986    9.222022

60.H         1.084884    1.810777    7.767600

61.H         0.082794    2.357228    9.152495

62.O        -0.908296    8.275590    4.965258

63.C        -1.974956    8.823483    4.164786

64.C         1.086581    6.259679    8.280212

65.C         0.822107    4.897416    8.898790

66.C         0.988896    2.563889    8.555894

67.H         1.015897    8.294191    6.620816

68.C         1.997744    4.448413    4.137838

69.O         0.987677   -1.361569    1.165033

70.O         2.815241    0.964795    1.844142

71.C         3.346782    2.245989    1.468076

72.H         4.384681    2.128958    1.107711

73.H         3.973926    4.064703    2.419083

74.H         3.827489    2.670451    3.531398

75.H         0.953521    4.727633    4.297095

76.H         2.604165    5.354709    3.968376

77.H         2.382367    3.934961    5.034973

78.H         4.034780   -0.112676    0.535938

79.H         2.429418    0.330640   -0.118555

80.H         2.748135   -1.547544    2.277677

81.H         2.835933   -2.143300    0.587293

82.C         3.360466    3.179763    2.668236

83.H         0.787586   -3.449618    1.308332

84.H        -0.647904   -2.460905    1.739035

85.H         0.734277   -2.549679    2.867411

86.O         2.024930    3.585384    2.993212

87.C         2.964596   -0.005757    0.785746

88.C         2.426874   -1.352876    1.240771

89.C         0.442931   -2.527399    1.806396

90.H         2.745707    2.686791    0.653980

91.C        -0.950603    4.308280    1.611587

92.O        -2.757370    1.661165    5.894764

93.O        -1.897565    4.074291    5.491536

94.C        -1.678590    5.462888    5.073692

95.H        -2.416777    6.108430    5.557610

96.H        -1.362317    6.351379    3.121369

97.H        -2.929356    5.507321    3.290261

98.H        -0.373552    3.403494    1.405280

99.H        -0.344465    5.192628    1.391980

100.H        -1.867915    4.351211    1.009464

101.H        -3.352713    4.210453    6.972381

102.H        -1.671465    4.369986    7.549629

103.H        -2.797575    2.048848    7.963175

104.H        -1.174782    2.043028    7.192755

105.C        -1.864444    5.486619    3.559489

106.H        -3.173691   -0.198739    6.764146

107.H        -1.497569   -0.012067    6.142077

108.H        -2.841345   -0.186298    4.990353

109.O        -1.274718    4.255120    3.031414

110.C        -2.332232    3.846002    6.853223

111.C        -2.222667    2.343405    7.074341

112.C        -2.554358    0.222661    5.960485

113.H        -0.672384    5.750885    5.379369

114.C        -3.887274    4.618427   -0.913370

115.O         1.303002    6.750290    0.530188

116.O        -1.451426    7.499407    1.018966

117.C        -2.676791    7.869900    0.376752

118.H        -3.192904    8.658435    0.955922

119.H        -4.594426    6.978607   -0.013444

120.H        -3.645118    6.140665    1.253433

121.H        -3.406035    3.994884   -1.673786

122.H        -4.890677    4.915949   -1.264008

123.H        -4.008100    4.038784    0.021061

124.H        -0.603647    9.395058    1.304339

125.H        -0.280714    8.631928   -0.287256

126.H         0.777764    7.556916    2.392671

127.H         1.682184    8.655648    1.306799

128.C        -3.578992    6.648617    0.274136

129.H         3.365954    7.043949    0.781955

130.H         2.826241    5.430249    0.210453

131.H         2.604619    5.884501    1.926556

132.O        -3.048722    5.753615   -0.708435

133.C        -0.386589    8.440447    0.792404

134.C         0.909768    7.865845    1.338948

135.C         2.599049    6.257524    0.891184

136.H        -2.480160    8.254844   -0.636844

137.C        -5.839529    3.433513    7.893144

138.H        -9.518941    1.993812    5.729265

139.H        -9.215533    3.749060    5.912458

140.C        -3.818078    3.635987   10.697403

141.O        -3.327486    4.500321    9.661235

142.O        -3.903475    6.451866    7.448511

143.C        -5.097825    7.227847    7.238378

144.H        -5.817318    7.069453    8.059834

145.H        -6.665626    7.421512    5.804434

146.H        -6.068694    5.746913    5.980389

147.H        -4.751096    7.154353    2.809802

148.H        -6.294090    7.743697    3.505808

149.H        -5.981818    5.984648    3.395945

150.H        -3.381118    7.782069    8.981565

151.H        -2.188620    6.524481    8.554093

152.H        -4.889618    5.877109    9.869887

153.H        -3.413352    6.245661   10.809859

154.C        -5.760660    6.802730    5.937398

155.H        -3.470735    3.968180   11.689573

156.H        -3.427770    2.632607   10.493166

157.H        -4.920548    3.607527   10.697013

158.O        -4.848250    7.017345    4.842936

159.C        -5.515375    6.965046    3.570898

160.C        -3.255650    6.721329    8.709070

161.C        -3.785062    5.853262    9.846108

162.H        -4.834681    8.298809    7.202770

163.C        -4.070540   -1.769118    3.162652

164.O        -2.723531   -2.114606    3.508120

165.O        -0.406831   -2.501659    5.314527

166.C         0.890049   -3.048849    5.621488

167.H         0.808423   -3.737646    6.480706

168.H         2.780810   -2.410951    6.380707

169.H         1.446526   -1.273109    6.734766

170.H         3.491278    0.190799    4.043550

171.H         4.224318   -0.936600    5.246027

172.H         3.142626    0.381033    5.796905

173.H        -1.342296   -4.348626    5.604445

174.H        -0.904119   -3.967214    3.912207

175.H        -3.039287   -2.474194    5.545480

176.H        -3.362278   -3.860532    4.462095

177.C         1.872018   -1.942756    5.962648

178.H        -4.667612   -2.670201    2.945380

179.H        -4.022080   -1.139065    2.270087

180.H        -4.562908   -1.209176    3.978287

181.O         2.195396   -1.197179    4.782686

182.C         3.332187   -0.343587    4.984836

183.C        -1.288146   -3.539952    4.853860

184.C        -2.690687   -3.002607    4.640230

185.H         1.273387   -3.617808    4.757584

Figure S4b1: Mg2+(DGM)3

NMR Shielding ADF-GUI atom  Mg(24):        566.87 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -3.804120    1.714903    1.110706

2.C        -2.937935    1.226140    0.024207

3.C        -1.992879    0.160844    0.596736

4.O        -0.748169    0.294719   -0.082162

5.C         0.135779   -0.818041    0.182133

6.C        -5.136342    2.111989    0.673711

7.C        -5.927884    2.451142    1.927963

8.O        -5.110456    3.363868    2.717762

9.C        -5.837710    3.973844    3.824195

10.H        -2.353717    2.065931   -0.368543

11.H        -3.573630    0.819044   -0.769197

12.H        -2.414180   -0.848045    0.451047

13.H        -1.874366    0.319978    1.684321

14.H        -0.327696   -1.765344   -0.132588

15.H         0.380561   -0.875358    1.256678

16.H         1.045682   -0.641482   -0.397871

17.H        -5.614127    1.282581    0.137124

18.H        -5.057102    2.980531    0.006145

19.H        -6.873034    2.940993    1.656257

20.H        -6.140461    1.554021    2.525852

21.H        -5.146317    4.669826    4.300919

22.H        -6.164146    3.195837    4.528059

23.H        -6.708846    4.513844    3.433745

24.Mg       -3.035466    3.153835    2.489146

25.H        -4.116365    6.607425    4.761389

26.H        -2.608764    9.660579    6.137149

27.H        -3.150602    8.302766    7.180533

28.H        -4.201640    8.882467    5.843919

29.H        -1.997482    4.062811    6.178063

30.H        -3.643348    3.450067    5.842931

31.H        -2.090057    1.487468    5.943435

32.H        -0.975924    2.300173    4.803065

33.C        -3.099402    6.545451    5.190124

34.H        -3.429826   -0.101365    4.867269

35.H        -4.206869    0.364797    3.316163

36.H        -4.595261    1.268608    4.823441

37.O        -2.484214    7.823063    5.245204

38.C        -2.624915    3.543375    5.443537

39.C        -2.022870    2.186013    5.100435

40.C        -3.814983    0.731291    4.267246

41.H        -2.257273    6.077885    3.259135

42.O        -2.713499    1.631984    3.930486

43.O        -2.682029    4.307616    4.196798

44.C        -3.157767    8.715490    6.159197

45.C        -2.207293    5.696622    4.280320

46.H        -1.174544    5.695735    4.653422

47.H        -3.167603    6.097810    6.199600

48.C        -4.049217    5.483348    0.515060

49.H        -2.994955    7.389590    0.448492

50.H        -4.257948    8.683315    3.586337

51.H        -4.945375    9.130315    1.984133

52.H        -3.164315    9.053462    2.223124

53.H        -1.829292    4.185407   -0.563862

54.H        -1.490384    5.833590    0.055661

55.H        -0.307517    4.983192    2.004941

56.H         0.299720    4.049573    0.595193

57.C        -3.963502    6.975677    0.785533

58.H         0.605127    1.828602    1.456393

59.H        -0.410672    1.361720    2.853826

60.H         0.691481    2.776371    2.994595

61.O        -4.149531    7.193223    2.182053

62.C        -1.703246    4.795993    0.341272

63.C        -0.578695    4.266673    1.216800

64.C         0.044762    2.197817    2.321414

65.H        -4.950361    5.076454    0.978509

66.O        -1.050821    3.037439    1.847217

67.O        -2.937326    4.732297    1.119527

68.C        -4.129820    8.606136    2.505183

69.H        -4.056801    5.286603   -0.565954

70.H        -4.755700    7.470717    0.193975

Figure S4b2: Mg2+(DGM)3(DGM)2

NMR Shielding ADF-GUI atom  Mg(24):        565.94 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -3.837678    1.083078    1.422522

2.C        -2.936112    0.465399    0.448115

3.C        -1.922198   -0.378512    1.228282

4.O        -0.723332   -0.432463    0.461887

5.C         0.281051   -1.233588    1.118980

6.C        -5.145676    1.451215    0.889257

7.C        -6.016833    1.837434    2.075790

8.O        -5.218378    2.691164    2.947849

9.C        -6.017891    3.378289    3.946098

10.H        -2.414281    1.247487   -0.115347

11.H        -3.532027   -0.146334   -0.239149

12.H        -2.320854   -1.394039    1.404431

13.H        -1.737977    0.086612    2.209424

14.H        -0.072453   -2.269634    1.248945

15.H         0.533106   -0.806985    2.104379

16.H         1.162680   -1.228538    0.471710

17.H        -5.585201    0.589751    0.370723

18.H        -5.040259    2.283671    0.185572

19.H        -6.888851    2.395639    1.707732

20.H        -6.336192    0.957474    2.652968

21.H        -5.330621    4.009622    4.512233

22.H        -6.503685    2.642454    4.602493

23.H        -6.763646    3.998569    3.438068

24.Mg       -3.155867    2.742705    2.606398

25.H        -4.030104    6.493631    4.639553

26.H        -2.237289    9.504822    5.660027

27.H        -2.859015    8.294464    6.831662

28.H        -3.888654    8.826617    5.460838

29.H        -2.067731    3.976900    6.189857

30.H        -3.616531    3.113867    5.965189

31.H        -1.756891    1.415251    6.051916

32.H        -0.875579    2.306872    4.783697

33.C        -3.000606    6.363718    5.015865

34.H        -3.157063   -0.299594    5.246278

35.H        -4.066810   -0.000892    3.724666

36.H        -4.382871    1.016175    5.169374

37.O        -2.271670    7.587696    4.941045

38.C        -2.642066    3.336527    5.511220

39.C        -1.866328    2.070611    5.178944

40.C        -3.619326    0.461325    4.607033

41.H        -2.360078    5.638149    3.087223

42.O        -2.585218    1.361092    4.114093

43.O        -2.896881    4.035429    4.247430

44.C        -2.853671    8.608736    5.775315

45.C        -2.262145    5.354710    4.135991

46.H        -1.206867    5.260986    4.412131

47.H        -3.048051    6.007786    6.062275

48.C        -4.664851    4.914913    0.775568

49.H        -3.769430    6.772685    0.047632

50.H        -3.765555    8.542916    3.183056

51.H        -5.129368    8.738924    2.017653

52.H        -3.433808    8.719796    1.433939

53.H        -2.640157    3.462498   -0.609004

54.H        -2.328743    5.205664   -0.349825

55.H        -0.713178    4.766737    1.436196

56.H        -0.300373    3.663806    0.083913

57.C        -4.527319    6.424464    0.773455

58.H         0.529121    1.813533    1.343134

59.H        -0.258785    1.436068    2.904279

60.H         0.553027    3.019298    2.699665

61.O        -4.180860    6.866820    2.090871

62.C        -2.385337    4.226168    0.140473

63.C        -1.064715    3.921805    0.830073

64.C        -0.014201    2.228413    2.199826

65.H        -5.401789    4.618870    1.517740

66.O        -1.282071    2.783258    1.711509

67.O        -3.413279    4.232540    1.167254

68.C        -4.129826    8.303436    2.180620

69.H        -4.972015    4.547991   -0.209613

70.H        -5.506489    6.830093    0.468825

71.C        -0.406851   -1.093796    4.949282

72.C         0.636938    6.672547    3.090465

73.O         0.380392    0.051981    4.603245

74.O         1.450432    2.819106    5.095535

75.C         2.381677    3.881520    4.795438

76.H         3.120341    3.957887    5.611869

77.H         2.461495    6.004168    4.689136

78.H         0.997533    5.392381    5.509958

79.H         0.128474    6.660356    2.119817

80.H         1.553146    7.278729    3.012016

81.H        -0.032396    7.115812    3.844018

82.H         2.949011    1.689274    6.011982

83.H         2.648320    1.298093    4.294617

84.H         0.621882    0.788918    6.548248

85.H         1.851984   -0.396075    6.016293

86.C         1.682927    5.223156    4.660413

87.H         0.233068   -1.954474    5.201731

88.H        -1.021641   -1.337157    4.077050

89.H        -1.059735   -0.880697    5.814299

90.O         0.964018    5.304332    3.413307

91.C         2.162458    1.573846    5.246448

92.C         1.234019    0.457650    5.690152

93.H         2.923049    3.654507    3.861114

94.C        -7.383005    6.566156    3.313068

95.C        -4.579391    2.105496   -2.536449

96.O        -7.350529    5.864789    2.058794

97.O        -7.722676    3.928977   -0.124119

98.C        -7.796610    3.673463   -1.542914

99.H        -8.820985    3.360055   -1.809154

100.H        -7.097412    2.272387   -2.991560

101.H        -6.957594    1.688339   -1.308242

102.H        -3.575503    2.541091   -2.485993

103.H        -4.849369    1.933292   -3.589770

104.H        -4.586182    1.137519   -2.005868

105.H        -9.679936    4.664811   -0.041395

106.H        -8.412308    5.891084   -0.340294

107.H        -8.794143    4.366947    2.307019

108.H        -9.436389    5.990114    1.926256

109.C        -6.840835    2.571536   -1.961680

110.H        -8.095081    7.405703    3.273999

111.H        -6.367046    6.937472    3.480704

112.H        -7.677142    5.897228    4.141307

113.O        -5.478117    3.041084   -1.920486

114.C        -8.654694    4.975559    0.225246

115.C        -8.617951    5.282099    1.712218

116.H        -7.561256    4.594130   -2.103000

Figure S4b3: Mg2+(DGM)3(DGM)4

NMR Shielding ADF-GUI atom  Mg(24):        563.54 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -1.764384    0.545564    1.257353

2.C        -0.431937    0.255827    0.733263

3.C         0.348846   -0.456812    1.837397

4.O         1.746511   -0.263606    1.584476

5.C         2.548839   -0.858816    2.620404

6.C        -2.858187    0.364906    0.300368

7.C        -4.153031    0.407273    1.092458

8.O        -4.059914    1.504786    2.062107

9.C        -5.336518    1.815932    2.678779

10.H         0.064032    1.199172    0.476983

11.H        -0.523332   -0.371403   -0.152673

12.H         0.096826   -1.530361    1.834491

13.H         0.081180   -0.029043    2.815564

14.H         2.366101   -1.945256    2.681392

15.H         2.326091   -0.399146    3.597992

16.H         3.596075   -0.681251    2.356653

17.H        -2.760978   -0.606995   -0.185341

18.H        -2.812399    1.157812   -0.453407

19.H        -5.000861    0.578396    0.422636

20.H        -4.302941   -0.526705    1.644640

21.H        -5.163457    2.669051    3.338242

22.H        -5.686238    0.945545    3.255678

23.H        -6.058978    2.075177    1.897127

24.Mg       -2.146928    2.161609    2.497415

25.H        -4.698459    5.082178    4.599824

26.H        -4.498450    8.700989    4.937636

27.H        -4.521317    7.585966    6.344387

28.H        -5.647135    7.320858    4.970257

29.H        -2.859228    3.322376    6.202037

30.H        -3.883781    2.092799    5.406575

31.H        -1.800832    0.973093    6.256916

32.H        -0.794671    2.190896    5.427989

33.C        -3.726742    5.498085    4.914033

34.H        -2.186250   -0.979731    4.996767

35.H        -2.417935   -0.810543    3.219074

36.H        -3.607863   -0.085328    4.349028

37.O        -3.632826    6.881677    4.572911

38.C        -2.920895    2.618531    5.365061

39.C        -1.744897    1.651685    5.395917

40.C        -2.548113   -0.330256    4.190955

41.H        -2.580137    5.115448    3.129239

42.O        -1.741074    0.880132    4.154309

43.O        -2.882293    3.332419    4.087020

44.C        -4.636792    7.662048    5.250806

45.C        -2.601576    4.771275    4.166776

46.H        -1.625253    4.914570    4.641284

47.H        -3.637316    5.372527    6.008517

48.C        -3.440730    3.956176    0.198029

49.H        -2.841491    5.827903   -0.780551

50.H        -3.636956    7.935858    2.124304

51.H        -4.847097    7.616567    0.833022

52.H        -3.163574    8.057372    0.391394

53.H        -0.694040    3.200919   -0.275212

54.H        -1.026871    4.948315   -0.035225

55.H        -0.158909    4.919000    2.242282

56.H         1.039403    4.054926    1.224790

57.C        -3.577916    5.452927   -0.045312

58.H         1.824740    2.328706    2.685366

59.H         0.685206    1.725518    3.925146

60.H         1.138800    3.457999    3.931138

61.O        -3.413313    6.133317    1.202451

62.C        -0.978325    3.970176    0.457179

63.C         0.010831    4.037241    1.612089

64.C         0.954752    2.578889    3.305721

65.H        -4.298511    3.594255    0.762796

66.O        -0.180871    2.845224    2.423214

67.O        -2.268035    3.622836    1.024439

68.C        -3.788408    7.519086    1.123844

69.H        -3.374583    3.421655   -0.755208

70.H        -4.586517    5.606784   -0.458889

71.C         0.508702   -0.912676    5.891585

72.C        -0.020158    6.942947    4.257394

73.O         1.053091    0.408927    5.813121

74.O         1.069257    3.327552    6.545139

75.C         1.728483    4.611641    6.557148

76.H         2.081969    4.828338    7.580343

77.H         1.268472    6.684707    6.418851

78.H        -0.169814    5.653342    6.668634

79.H        -0.136075    6.867060    3.170994

80.H         0.633257    7.796987    4.496555

81.H        -1.011385    7.101977    4.711389

82.H         2.358414    2.582877    8.009373

83.H         2.839551    2.228609    6.324937

84.H         0.327901    1.069972    7.661516

85.H         1.936015    0.285805    7.701567

86.C         0.793403    5.730589    6.132839

87.H         1.205700   -1.600179    6.398204

88.H         0.337078   -1.250569    4.864996

89.H        -0.446703   -0.915223    6.446084

90.O         0.576681    5.709126    4.708918

91.C         1.977802    2.309268    7.009913

92.C         1.285935    0.962875    7.121261

93.H         2.605779    4.592139    5.887834

94.C        -6.382019    5.681451    2.615070

95.C        -4.120154    3.865846   -3.382217

96.O        -6.293782    4.888802    1.427999

97.O        -6.778085    2.498395   -0.276226

98.C        -6.660076    1.847471   -1.563845

99.H        -6.703534    0.769814   -1.373500

100.H        -5.323727    1.579133   -3.220908

101.H        -4.491082    1.807062   -1.673310

102.H        -4.131797    4.948308   -3.548184

103.H        -4.196088    3.341796   -4.349054

104.H        -3.168990    3.567039   -2.909915

105.H        -8.482511    3.602557   -0.758670

106.H        -6.929062    4.445909   -1.040528

107.H        -7.960925    3.659947    1.746286

108.H        -8.299687    5.228900    0.954860

109.C        -5.346763    2.149609   -2.273981

110.H        -7.095343    6.513945    2.484134

111.H        -5.382010    6.079386    2.803550

112.H        -6.719600    5.074506    3.476101

113.O        -5.238148    3.558436   -2.539695

114.C        -7.465222    3.766974   -0.362894

115.C        -7.579117    4.394009    1.012946

116.H        -7.508256    2.133631   -2.205250

117.C        -2.074268   -3.502406   -0.623536

118.O        -0.859187   -2.736743   -0.493664

119.C        -3.796244   -3.123130    2.652748

120.C         2.115691    0.088770   -1.824216

121.O        -3.179688   -2.729859    1.420486

122.C         0.050221   -2.987245   -1.588865

123.H         0.357132   -4.046582   -1.569096

124.H         2.090819   -2.540640   -2.078937

125.H         1.621243   -2.066770   -0.415178

126.H         1.806955    1.064758   -2.214941

127.H         2.957365   -0.290937   -2.426914

128.H         2.429476    0.184581   -0.773262

129.H        -1.868038   -4.448607   -1.150961

130.H        -2.816550   -2.927664   -1.198924

131.H        -1.842238   -4.338642    1.355862

132.H        -3.434323   -4.625320    0.587089

133.C         1.282393   -2.106729   -1.464731

134.H        -4.589976   -3.869426    2.479999

135.H        -4.240716   -2.225775    3.096158

136.H        -3.056932   -3.551456    3.351016

137.O         0.975925   -0.782358   -1.934914

138.C        -2.633392   -3.878651    0.739153

139.H        -0.445466   -2.787049   -2.553753

140.O        -4.183666   -1.150688   -2.070914

141.C        -6.987768   -1.549321    1.081992

142.C        -0.984758    1.719440   -2.665032

143.O        -6.490572   -1.232771   -0.221949

144.C        -3.514079   -0.924272   -3.324879

145.H        -3.371776   -1.889262   -3.843530

146.H        -1.538227   -0.439376   -4.003921

147.H        -1.628047   -0.825441   -2.267163

148.H        -1.163569    2.794508   -2.547147

149.H        -0.364262    1.551571   -3.560383

150.H        -0.442089    1.324638   -1.793582

151.H        -5.112542   -2.875305   -2.795311

152.H        -6.135288   -1.408722   -2.791178

153.H        -5.068901   -2.758863   -0.244464

154.H        -6.649253   -3.164032   -1.002059

155.C        -2.143718   -0.309065   -3.090713

156.H        -7.770627   -2.324762    1.033223

157.H        -7.413096   -0.627450    1.492835

158.H        -6.173997   -1.907760    1.736496

159.O        -2.268812    1.097966   -2.801105

160.C        -5.362875   -1.960135   -2.229329

161.C        -5.894020   -2.369548   -0.864824

162.H        -4.121772   -0.270888   -3.972937

Figure S4b4: Mg2+(DGM)3(DGM)6

NMR Shielding ADF-GUI atom  Mg(24):        563.38 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -1.716467    0.525107    1.255042

2.C        -0.384364    0.294016    0.702443

3.C         0.412565   -0.484366    1.746267

4.O         1.795640   -0.448182    1.363358

5.C         2.623732   -1.088198    2.348810

6.C        -2.826232   -0.028886    0.469282

7.C        -4.066891    0.019383    1.342415

8.O        -4.064197    1.300368    2.051162

9.C        -5.328271    1.573295    2.715559

10.H         0.081001    1.266288    0.509683

11.H        -0.463254   -0.271175   -0.228227

12.H         0.050642   -1.524842    1.787814

13.H         0.281963   -0.011906    2.731371

14.H         2.343273   -2.149114    2.465469

15.H         2.530519   -0.581796    3.324063

16.H         3.657288   -1.022738    1.994105

17.H        -2.597812   -1.061836    0.198871

18.H        -2.961055    0.573213   -0.431736

19.H        -4.966415   -0.055619    0.723716

20.H        -4.066868   -0.787651    2.084342

21.H        -5.253978    2.579628    3.124333

22.H        -5.483501    0.848485    3.529051

23.H        -6.152346    1.498630    1.999846

24.Mg       -2.207975    2.137298    2.452415

25.H        -4.575443    5.503544    4.047699

26.H        -3.844911    8.750087    5.498683

27.H        -4.587052    7.406084    6.429255

28.H        -5.155813    7.766247    4.765497

29.H        -2.993604    3.278197    6.175566

30.H        -3.870925    1.962881    5.348111

31.H        -1.670328    1.077890    6.242265

32.H        -0.799287    2.349327    5.351427

33.C        -3.725366    5.542738    4.744752

34.H        -2.051078   -0.886292    5.112596

35.H        -2.188226   -0.872869    3.320637

36.H        -3.478894   -0.134501    4.318320

37.O        -3.253355    6.886008    4.892533

38.C        -2.965716    2.581820    5.329259

39.C        -1.701149    1.731177    5.360088

40.C        -2.398327   -0.322549    4.238948

41.H        -2.376383    5.042199    3.147546

42.O        -1.663309    0.923242    4.143772

43.O        -2.995279    3.312783    4.064521

44.C        -4.274113    7.746037    5.427716

45.C        -2.574854    4.717783    4.169109

46.H        -1.665008    4.781045    4.778918

47.H        -4.045310    5.144337    5.726896

48.C        -3.669191    4.039512    0.354049

49.H        -3.079793    6.053903   -0.242058

50.H        -4.344993    7.782172    2.670282

51.H        -5.450648    7.466133    1.279944

52.H        -3.773999    8.044448    0.997281

53.H        -0.905698    3.329252   -0.263204

54.H        -1.302936    5.054440    0.051832

55.H        -0.360422    5.005477    2.257941

56.H         0.826924    4.214135    1.162704

57.C        -3.883151    5.540617    0.310178

58.H         1.743432    2.451296    2.538036

59.H         0.684674    1.773622    3.817845

60.H         1.101544    3.513970    3.853394

61.O        -3.947379    6.060840    1.648089

62.C        -1.197991    4.066379    0.494327

63.C        -0.170878    4.148282    1.605350

64.C         0.897592    2.652490    3.208769

65.H        -4.490802    3.544785    0.873138

66.O        -0.285063    2.919093    2.398675

67.O        -2.461244    3.650398    1.099777

68.C        -4.411609    7.417219    1.640935

69.H        -3.602747    3.658540   -0.669534

70.H        -4.831295    5.698648   -0.218607

71.C         0.695888   -1.117412    5.541073

72.C         0.230671    6.730972    4.470583

73.O         1.095248    0.255804    5.622733

74.O         1.060782    3.050884    6.687755

75.C         1.656182    4.346001    6.907005

76.H         1.850692    4.482767    7.985586

77.H         1.154054    6.412749    6.804523

78.H        -0.274327    5.338965    6.839505

79.H         0.288616    6.662654    3.381442

80.H         0.868309    7.560650    4.819146

81.H        -0.810363    6.923289    4.769966

82.H         2.342893    2.172965    8.084263

83.H         2.868125    2.044674    6.379901

84.H         0.396371    0.641838    7.555540

85.H         2.032032   -0.077512    7.461357

86.C         0.743421    5.460267    6.426671

87.H         1.505357   -1.785005    5.881235

88.H         0.461824   -1.325169    4.493596

89.H        -0.195416   -1.310417    6.164010

90.O         0.706332    5.476316    4.991281

91.C         1.990755    2.014654    7.049133

92.C         1.343655    0.643441    6.986088

93.H         2.617720    4.413247    6.369946

94.C        -6.911534    5.310462    2.551476

95.C        -2.585990    4.950395   -3.873183

96.O        -6.952490    5.390787    1.124964

97.O        -6.099303    4.053931   -1.467677

98.C        -6.053886    4.268884   -2.881806

99.H        -6.806764    3.632672   -3.385321

100.H        -4.762350    3.995355   -4.545907

101.H        -4.436058    2.856903   -3.205883

102.H        -1.867706    5.634950   -3.411066

103.H        -2.943115    5.380759   -4.823546

104.H        -2.085655    3.990915   -4.086425

105.H        -8.091324    3.462546   -1.360883

106.H        -7.817546    5.234471   -1.275681

107.H        -6.833358    3.309408    0.885647

108.H        -8.478120    3.990691    0.893710

109.C        -4.691606    3.900160   -3.449061

110.H        -7.909571    5.094344    2.969539

111.H        -6.555577    6.277504    2.918925

112.H        -6.222793    4.516803    2.883505

113.O        -3.666612    4.788140   -2.944320

114.C        -7.432271    4.249985   -0.958472

115.C        -7.439536    4.165037    0.557176

116.H        -6.285050    5.323467   -3.113244

117.C         0.831038    5.008977   -2.121197

118.O         0.698871    5.942093   -1.039215

119.C         2.791356    2.490843   -0.249239

120.C        -1.253774    8.309024    1.976369

121.O         1.632770    3.125892   -0.817644

122.C        -0.243904    6.983854   -1.338656

123.H         0.072324    7.525447   -2.247738

124.H        -0.876767    8.859074   -0.522713

125.H         0.693583    8.281132    0.116991

126.H        -1.825270    7.790677    2.750599

127.H        -1.838890    9.164251    1.598833

128.H        -0.306581    8.688225    2.395675

129.H         1.034718    5.547782   -3.063891

130.H        -0.102374    4.433912   -2.249169

131.H         2.860418    4.676375   -1.508590

132.H         2.275104    3.539732   -2.762161

133.C        -0.321628    7.966347   -0.181335

134.H         3.396175    2.000670   -1.029781

135.H         2.435444    1.730730    0.452304

136.H         3.420756    3.231355    0.271917

137.O        -1.007107    7.360752    0.926125

138.C         1.996175    4.075046   -1.836640

139.H        -1.245675    6.556538   -1.523054

140.O        -4.137792   -1.820776   -1.643307

141.C        -6.648737   -2.245216    1.730038

142.C        -1.917237    1.737157   -2.492746

143.O        -6.291993   -2.040435    0.358051

144.C        -3.792509   -1.438620   -2.987425

145.H        -3.509596   -2.337277   -3.564936

146.H        -2.160433   -0.465388   -3.988994

147.H        -1.840509   -0.835604   -2.278110

148.H        -2.320872    2.718354   -2.225969

149.H        -1.357618    1.812841   -3.440397

150.H        -1.223816    1.389918   -1.710822

151.H        -4.820275   -3.735934   -2.125910

152.H        -6.062967   -2.451258   -2.172414

153.H        -4.650557   -3.321783    0.411468

154.H        -6.177308   -4.055074   -0.186056

155.C        -2.609273   -0.483897   -2.980651

156.H        -7.275484   -3.146391    1.845591

157.H        -7.210818   -1.359616    2.046377

158.H        -5.746212   -2.361212    2.354073

159.O        -3.036852    0.849098   -2.625144

160.C        -5.175800   -2.816121   -1.627187

161.C        -5.555261   -3.141416   -0.190672

162.H        -4.660932   -0.970881   -3.482167

163.C        -9.288644    1.348939    3.222556

164.O        -8.507648    0.818325    2.140963

165.C        -6.707014    2.623735    5.555951

166.C        -6.311927    0.845454   -1.476202

167.O        -7.511606    2.498147    4.385093

168.C        -9.176346    0.984853    0.877152

169.H       -10.138777    0.442454    0.879423

170.H        -8.882206    0.560321   -1.192343

171.H        -8.102804   -0.628187   -0.106371

172.H        -5.423331    1.479542   -1.464312

173.H        -6.886456    1.048151   -2.398325

174.H        -6.015511   -0.211120   -1.452045

175.H       -10.170968    0.709826    3.404088

176.H        -9.642538    2.364998    2.976376

177.H        -7.904292    0.455864    4.626433

178.H        -9.110402    1.563269    5.355668

179.C        -8.314349    0.441282   -0.249928

180.H        -7.321818    2.816433    6.451555

181.H        -6.026711    3.466794    5.390161

182.H        -6.113246    1.706249    5.731195

183.O        -7.089283    1.184114   -0.316149

184.C        -8.446701    1.409378    4.486862

185.H        -9.382646    2.055646    0.712634

186.C        -1.827365   -3.919790   -0.061293

187.O        -0.722507   -3.015565   -0.232719

188.C        -3.290646   -3.328566    3.306293

189.C         1.647757    0.018071   -2.100802

190.O        -2.799034   -3.004426    1.999722

191.C        -0.127947   -3.186288   -1.537808

192.H         0.222678   -4.227909   -1.640158

193.H         1.719116   -2.642273   -2.494995

194.H         1.616572   -2.178070   -0.764187

195.H         1.200905    1.002317   -2.273701

196.H         2.374435   -0.212551   -2.898479

197.H         2.160827    0.022796   -1.129198

198.H        -1.566844   -4.907988   -0.480875

199.H        -2.709191   -3.533056   -0.594152

200.H        -1.214393   -4.374444    1.962038

201.H        -2.810581   -5.022256    1.476448

202.C         1.051758   -2.245052   -1.710025

203.H        -3.962299   -4.202529    3.271331

204.H        -3.853854   -2.461826    3.666647

205.H        -2.463442   -3.547051    4.003357

206.O         0.578224   -0.942040   -2.092405

207.C        -2.141209   -4.145911    1.408345

208.H        -0.875921   -2.995114   -2.326515

Table S3: Mg(BH4)(TFSI)(DGM)-1

NMR Shielding ADF-GUI atom  Mg(24):        548.20 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -0.643278    1.359463   -0.835967

2.C         0.805845    1.279481   -0.944007

3.C         1.199333   -0.053113   -0.322388

4.O         0.626593   -0.089283    1.007085

5.C         0.857467   -1.346236    1.700834

6.C        -1.192352    2.663412   -1.205497

7.C        -2.666548    2.643851   -0.820639

8.O        -2.762616    2.139807    0.534771

9.C        -4.110936    2.152210    1.068875

10.H         1.251096    2.118415   -0.394411

11.H         1.107063    1.316008   -2.000263

12.H         2.294746   -0.135330   -0.261564

13.H         0.797374   -0.894352   -0.909019

14.H         0.276999   -1.300661    2.624007

15.H         1.931261   -1.454284    1.904977

16.H         0.492838   -2.181446    1.086954

17.H        -1.083610    2.817684   -2.287962

18.H        -0.664364    3.442104   -0.649420

19.H        -3.249231    1.982729   -1.481319

20.H        -3.060771    3.668668   -0.863741

21.H        -4.438978    3.192030    1.195865

22.H        -4.067933    1.626818    2.025211

23.H        -4.783864    1.613050    0.386630

24.Mg       -1.176712    0.992336    1.213341

25.F        -1.918752    2.379379    4.222917

26.F        -2.490791    4.198139    3.121616

27.F        -1.390416    4.366370    5.023271

28.F         1.578563    4.569781   -0.230529

29.F         2.431194    6.405634    0.646040

30.B        -2.401738   -0.717277    2.275557

31.H        -3.572281   -0.477327    2.469281

32.H        -2.020291   -1.780828    2.706778

33.H        -2.181599   -0.700419    1.042268

34.H        -1.721942    0.171889    2.851946

35.N         0.480286    5.055197    2.593827

36.S         0.141221    3.555848    2.955993

37.S        -0.150494    5.922786    1.370880

38.C        -1.528178    3.640032    3.898431

39.C         1.310476    5.868931    0.128902

40.O        -0.240575    7.314252    1.769984

41.O        -1.249808    5.291736    0.637690

42.O        -0.205074    2.676777    1.794015

43.O         1.093340    3.017534    3.907889

44.F         0.972187    6.547598   -0.996240

Table S3: Mg(BH4)(TFSI)(DGM)-1 + 2 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        549.84 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -0.683677    1.386980   -0.957533

2.C         0.694666    1.123884   -1.321554

3.C         1.087919   -0.121247   -0.542887

4.O         0.818309    0.150259    0.857723

5.C         1.099222   -0.984746    1.720819

6.C        -1.201902    2.669857   -1.433955

7.C        -2.635120    2.786102   -0.922739

8.O        -2.683314    2.229768    0.423127

9.C        -3.946182    2.432350    1.092393

10.H         1.316547    1.982944   -1.032925

11.H         0.756835    0.952086   -2.400907

12.H         2.157030   -0.343738   -0.677074

13.H         0.486562   -0.986522   -0.865136

14.H         0.896569   -0.654685    2.742269

15.H         2.154380   -1.271456    1.611758

16.H         0.432138   -1.819418    1.468894

17.H        -1.172973    2.683992   -2.527354

18.H        -0.574902    3.465161   -1.018380

19.H        -3.324786    2.217109   -1.556086

20.H        -2.912711    3.847838   -0.882728

21.H        -4.085743    3.501867    1.295725

22.H        -3.901901    1.856905    2.020149

23.H        -4.762634    2.049585    0.462713

24.Mg       -1.080614    1.120055    1.076887

25.F        -1.920359    2.406217    4.428416

26.F        -2.547972    4.216440    3.339020

27.F        -1.400090    4.401005    5.211446

28.F         1.554239    4.276995    0.003268

29.F         2.392721    6.202796    0.668007

30.B        -2.248758   -0.686802    2.029061

31.H        -3.441447   -0.477223    1.961070

32.H        -1.938255   -1.714967    2.585710

33.H        -1.780408   -0.723426    0.871279

34.H        -1.716771    0.248780    2.675646

35.N         0.330597    5.129260    2.689394

36.S         0.081879    3.618557    3.101141

37.S        -0.224563    5.848441    1.341652

38.C        -1.557213    3.670060    4.090498

39.C         1.285449    5.610423    0.181328

40.O        -0.284260    7.280762    1.566052

41.O        -1.311054    5.163717    0.641570

42.O        -0.248905    2.702632    1.974680

43.O         1.078404    3.154694    4.047371

44.F         1.008185    6.139170   -1.044035

45.O        -3.358216    0.116845   -2.695912

46.O        -0.775213    0.617677   -4.252808

47.C        -0.238987    1.344526   -5.365775

48.H        -0.018817    0.656382   -6.203421

49.H         1.544373    2.456898   -5.836348

50.H         1.739667    1.273151   -4.506684

51.H         1.636092    4.394015   -2.730078

52.H         2.525579    4.155027   -4.274840

53.H         2.604021    2.906237   -2.988029

54.H        -1.624660   -0.939950   -5.346533

55.H        -2.685265    0.483749   -5.102632

56.H        -1.718163   -1.180803   -2.731706

57.H        -3.131469   -1.690375   -3.708335

58.C         1.054369    2.023712   -4.944808

59.H        -4.536052   -1.335745   -1.737665

60.H        -4.529869    0.310835   -1.028774

61.H        -3.118480   -0.756389   -0.793869

62.O         0.764758    3.045638   -3.987050

63.C         1.954102    3.657637   -3.472248

64.C        -1.926830   -0.159703   -4.623850

65.C        -2.528779   -0.818292   -3.390528

66.C        -3.908802   -0.458915   -1.498395

67.H        -0.966152    2.097586   -5.716387

Table S3: Mg(BH4)(TFSI)(DGM)-1 + 4 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        549.45 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -2.460735    1.884852    0.561538

2.C        -1.667398    1.711528   -0.641906

3.C        -1.732446    0.226716   -0.968938

4.O        -1.432402   -0.504660    0.247724

5.C        -1.425846   -1.941488    0.074190

6.C        -2.411985    3.240679    1.118471

7.C        -3.218182    3.211658    2.407491

8.O        -2.872789    1.976931    3.122069

9.C        -3.581733    1.839864    4.373421

10.H        -0.639044    2.029000   -0.438641

11.H        -2.097011    2.314803   -1.449697

12.H        -0.991639   -0.024372   -1.742874

13.H        -2.738726   -0.062711   -1.311959

14.H        -1.332865   -2.376095    1.071830

15.H        -0.581561   -2.226577   -0.569579

16.H        -2.375277   -2.269130   -0.374373

17.H        -2.853035    3.936305    0.399539

18.H        -1.364133    3.497039    1.301087

19.H        -4.293343    3.191153    2.195056

20.H        -2.951268    4.071012    3.029266

21.H        -3.290451    2.654829    5.045738

22.H        -3.313738    0.862549    4.781670

23.H        -4.666179    1.872426    4.187037

24.Mg       -1.987374    0.470561    2.034018

25.F        -0.667918    2.485603    4.993549

26.F        -0.031878    3.899612    3.417858

27.F         1.332912    3.392385    5.071147

28.F         1.417880    0.410102   -0.113125

29.F         3.610124    0.591754   -0.011646

30.B        -3.014736   -1.403668    3.071806

31.H        -3.669973   -1.249020    4.079437

32.H        -2.922562   -2.553377    2.700237

33.H        -3.542382   -0.740366    2.152990

34.H        -1.851616   -0.989700    3.299521

35.N         2.329664    2.011168    2.462957

36.S         1.053089    1.436997    3.229312

37.S         2.289830    2.736667    1.017893

38.C         0.377512    2.915332    4.242010

39.C         2.465023    1.273911   -0.215318

40.O         3.516899    3.495462    0.841081

41.O         1.010404    3.347383    0.644115

42.O        -0.095261    1.114682    2.340258

43.O         1.444292    0.449644    4.215291

44.F         2.470880    1.774917   -1.484217

45.O        -5.590686    2.329218    0.372047

46.O        -4.210330    3.698099   -1.952088

47.C        -3.823170    4.981812   -2.454600

48.H        -4.470889    5.274325   -3.302156

49.H        -2.143372    5.861114   -3.471125

50.H        -2.280210    4.085429   -3.665586

51.H         0.460707    4.469112   -1.352494

52.H         0.190448    5.475799   -2.817368

53.H        -0.024899    3.696542   -2.897777

54.H        -6.199482    3.769784   -2.574730

55.H        -5.886903    4.454321   -0.947252

56.H        -5.375215    1.506881   -1.538699

57.H        -7.020249    2.088376   -1.131449

58.C        -2.386544    4.918115   -2.945371

59.H        -6.606878    0.574248    0.928879

60.H        -5.278186    1.131342    2.001289

61.H        -4.889825    0.354980    0.444947

62.O        -1.507949    4.730046   -1.834250

63.C        -0.142349    4.586157   -2.254171

64.C        -5.613869    3.643636   -1.645332

65.C        -5.940292    2.298827   -1.013388

66.C        -5.598319    1.023198    0.960895

67.H        -3.921862    5.746821   -1.663535

68.C         3.410678    5.466043    3.772796

69.O        -2.363000    9.020843    6.976126

70.O        -0.049191    8.372921    5.318573

71.C         1.337135    8.273350    4.958435

72.H         1.551562    8.930201    4.097188

73.H         0.962040    6.493272    3.780036

74.H         1.499608    6.163689    5.454776

75.H         4.426775    5.538438    3.372511

76.H         2.752301    5.045915    2.997796

77.H         3.399786    4.797881    4.648080

78.H        -0.057687   10.433648    4.986403

79.H         0.100090    9.933066    6.699991

80.H        -2.380273    9.483313    4.939100

81.H        -2.160163   10.879305    6.042968

82.C         1.638629    6.824718    4.582549

83.H        -4.150984   10.088999    7.246911

84.H        -4.065472    8.432805    7.938286

85.H        -4.263956    8.657741    6.168161

86.O         3.002148    6.794481    4.133461

87.C        -0.391020    9.694188    5.739390

88.C        -1.899922    9.816683    5.876928

89.C        -3.788843    9.057810    7.082386

90.H         1.978120    8.584980    5.801601

91.C         1.649469    6.936680    1.080662

92.O        -2.190790    5.264345    4.922896

93.O        -2.576893    6.296092    2.128887

94.C        -2.074188    6.822687    0.888864

95.H        -2.686314    6.366893    0.101185

96.H        -0.440948    6.722919   -0.492664

97.H        -0.444165    5.406697    0.707342

98.H         2.276580    7.441637    1.821541

99.H         1.895996    7.291201    0.062968

100.H         1.833953    5.853345    1.126750

101.H        -2.450533    8.111583    3.150616

102.H        -1.049085    7.040406    3.369194

103.H        -3.863762    6.419873    4.429557

104.H        -2.566235    7.263162    5.347489

105.C        -0.618664    6.484187    0.572907

106.H        -2.173299    5.709158    6.968338

107.H        -2.011731    3.981788    6.502368

108.H        -3.609816    4.794055    6.401839

109.O         0.279162    7.239226    1.400461

110.C        -2.138075    7.057844    3.278128

111.C        -2.769079    6.531865    4.552247

112.C        -2.518216    4.925042    6.273858

113.H        -2.209695    7.919526    0.862413

Table S3: Mg(BH4)(TFSI)(DGM)-1 + 6 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        547.99 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -1.926966    1.641757    2.053659

2.C        -0.643276    1.965791    1.441727

3.C         0.334586    0.978726    2.043681

4.O         0.147318    1.013303    3.493522

5.C         1.049431    0.110523    4.187393

6.C        -3.066972    2.404553    1.571186

7.C        -4.229846    1.922929    2.420400

8.O        -3.814162    1.995171    3.811474

9.C        -4.855171    1.491862    4.705221

10.H        -0.385947    3.001782    1.694848

11.H        -0.715457    1.845305    0.357202

12.H         1.368620    1.248372    1.815508

13.H         0.143034   -0.041229    1.692037

14.H         0.775924    0.148883    5.243720

15.H         2.076909    0.438610    4.008865

16.H         0.913825   -0.909322    3.804340

17.H        -3.225106    2.191090    0.507275

18.H        -2.872005    3.474572    1.715035

19.H        -4.473821    0.874512    2.183578

20.H        -5.118961    2.549226    2.277598

21.H        -5.734332    2.132719    4.628103

22.H        -4.440343    1.501305    5.711597

23.H        -5.097444    0.459751    4.426139

24.Mg       -1.779368    1.558909    4.108845

25.F        -3.222460    3.521169    6.598783

26.F        -3.747503    5.148749    5.209873

27.F        -2.843999    5.620300    7.158724

28.F         0.829066    5.026825    2.426128

29.F         1.287630    7.168621    2.685650

30.B        -2.098589   -0.263301    5.590690

31.H        -3.125771   -0.500520    6.178840

32.H        -1.181783   -1.008187    5.844769

33.H        -2.328408   -0.320947    4.370740

34.H        -1.748716    0.897278    5.914409

35.N        -0.854617    6.026189    4.702554

36.S        -1.106437    4.611850    5.359633

37.S        -1.285557    6.477743    3.201077

38.C        -2.849907    4.742135    6.133814

39.C         0.363301    6.290910    2.258296

40.O        -1.592426    7.895424    3.199048

41.O        -2.185275    5.557162    2.507734

42.O        -1.273156    3.490628    4.394614

43.O        -0.203469    4.377395    6.468353

44.F         0.124177    6.506617    0.944157

45.O        -2.412436   -0.832679    0.394225

46.O        -1.068492    0.731456   -1.673658

47.C        -1.527082    1.582507   -2.735622

48.H        -1.084582    1.266825   -3.698394

49.H        -1.434438    3.647009   -3.304899

50.H        -0.034657    3.106176   -2.342248

51.H        -2.084000    5.128485   -0.097347

52.H        -2.273031    5.410343   -1.856107

53.H        -0.648418    5.234183   -1.163521

54.H        -0.918982   -1.143552   -2.586145

55.H        -2.577083   -0.630738   -2.142579

56.H        -0.397936   -1.205378   -0.056850

57.H        -1.558834   -2.429024   -0.655223

58.C        -1.130653    3.020220   -2.446233

59.H        -2.560632   -2.566253    1.562478

60.H        -3.189418   -1.040607    2.272265

61.H        -1.437562   -1.316560    2.189513

62.O        -1.777246    3.454878   -1.248289

63.C        -1.685869    4.891802   -1.086819

64.C        -1.521426   -0.620902   -1.821175

65.C        -1.404873   -1.344674   -0.489454

66.C        -2.391634   -1.479430    1.668075

67.H        -2.625342    1.508111   -2.815121

68.C         2.578646    3.325815    4.238951

69.O         1.621277   -2.036535    1.473589

70.O         3.691449    0.039467    2.020615

71.C         4.314481    1.288616    1.680858

72.H         5.379992    1.129449    1.429837

73.H         4.776185    3.158974    2.663110

74.H         4.616031    1.756094    3.769720

75.H         1.496367    3.350982    4.380328

76.H         2.959705    4.344424    4.111785

77.H         3.047997    2.847423    5.115999

78.H         4.703380   -1.068938    0.567561

79.H         3.099767   -0.440081    0.073374

80.H         3.477069   -2.502929    2.314456

81.H         3.271554   -2.962364    0.594601

82.C         4.201681    2.236953    2.863813

83.H         1.195712   -4.077671    1.241035

84.H        -0.067212   -3.054581    2.004921

85.H         1.392382   -3.522128    2.936089

86.O         2.820805    2.539483    3.057066

87.C         3.671634   -0.871581    0.915426

88.C         3.043651   -2.186219    1.348804

89.C         1.007851   -3.243871    1.940118

90.H         3.813379    1.727912    0.800775

91.C         2.844938    6.122400    6.303326

92.O         2.416653    4.941745   -0.002231

93.O         4.199782    5.781955    2.329884

94.C         4.580455    6.914456    3.128183

95.H         5.633630    7.182407    2.919457

96.H         4.964799    7.340328    5.203783

97.H         4.913137    5.594953    4.807653

98.H         1.764314    6.072007    6.459790

99.H         3.302121    6.839407    7.008455

100.H         3.284178    5.124135    6.477571

101.H         5.426007    6.214642    0.697869

102.H         3.793171    6.951683    0.642170

103.H         4.121476    3.928073    0.665478

104.H         4.314010    4.834230   -0.865039

105.C         4.438082    6.573939    4.603149

106.H         2.163846    3.102015   -0.993735

107.H         0.715432    3.838473   -0.246002

108.H         1.957466    3.072739    0.794148

109.O         3.054893    6.536853    4.947654

110.C         4.356394    6.045499    0.928522

111.C         3.841508    4.851356    0.135625

112.C         1.785201    3.659210   -0.117930

113.H         3.941084    7.779550    2.882080

114.C        -4.511296    6.961777    0.247666

115.O         0.774870    5.972078   -3.211441

116.O        -0.813968    7.830418   -1.536928

117.C        -1.757909    8.882441   -1.300700

118.H        -1.224860    9.789792   -0.959954

119.H        -3.294735    9.340093    0.132522

120.H        -2.189587    8.030720    0.634411

121.H        -5.171322    6.233399   -0.236334

122.H        -5.122979    7.763499    0.701238

123.H        -3.930108    6.470040    1.041505

124.H         0.648953    9.166579   -2.179805

125.H        -0.271841    8.356064   -3.484632

126.H         1.613827    6.893140   -1.537623

127.H         2.120187    7.567240   -3.124446

128.C        -2.736693    8.452685   -0.223003

129.H         2.582998    5.455086   -4.135235

130.H         1.389867    4.137931   -3.870735

131.H         2.338529    4.784002   -2.488557

132.O        -3.649183    7.487038   -0.767386

133.C         0.180861    8.211086   -2.486392

134.C         1.267833    7.153039   -2.551874

135.C         1.836094    5.038440   -3.434755

136.H        -2.299984    9.126949   -2.232138

137.C        -6.309886   -1.150150    6.318687

138.H        -9.663006    1.874909    6.214320

139.H        -8.122038    2.270701    7.040581

140.H        -8.390614   -0.119453    5.144010

141.H        -8.771610   -0.230863    6.891961

142.C        -7.713964    4.460945    3.725138

143.H        -6.814948   -1.809668    7.046512

144.H        -5.232280   -1.132142    6.510567

145.H        -6.494623   -1.540356    5.301383

146.O        -6.286486    4.367751    3.757917

147.C        -8.562566    1.783869    6.152644

148.C        -8.172863    0.314340    6.137801

149.H        -7.791836    4.268304    5.871160

150.C        -5.673812    5.091930    2.684507

151.O        -6.779144    0.197523    6.436215

152.O        -8.087466    2.416718    4.955397

153.C        -8.288630    3.835197    4.984939

154.H        -9.369191    4.065840    5.042488

155.H        -8.023884    5.521852    3.686069

156.H        -8.111908    3.951154    2.828164

157.H        -4.592258    4.994119    2.800177

158.H        -5.949487    6.159126    2.723074

159.H        -5.983581    4.686682    1.704923

Table S3: Mg(BH4)(TFSI)(DGM)-2

NMR Shielding ADF-GUI atom  Mg(24):        559.66 ppm

Atom         X           Y           Z   (Angstrom)

1.O         0.316577   -0.044188    0.289386

2.C         1.745253    0.160373    0.476698

3.C         2.092098   -0.560577    1.770551

4.O         1.210700   -0.029309    2.791215

5.C         1.379626   -0.665010    4.083983

6.C        -0.257220    0.685558   -0.831728

7.C        -1.766705    0.614093   -0.652690

8.O        -2.063062    1.097785    0.685190

9.C        -3.487786    1.112737    0.968508

10.H         1.945825    1.237107    0.544553

11.H         2.298057   -0.277606   -0.366457

12.H         3.138251   -0.367896    2.049658

13.H         1.919659   -1.643913    1.676661

14.H         0.676611   -0.172931    4.760731

15.H         2.409127   -0.512478    4.433742

16.H         1.142269   -1.734583    4.005783

17.H         0.036329    0.202230   -1.774788

18.H         0.105195    1.717807   -0.810554

19.H        -2.128906   -0.421539   -0.738060

20.H        -2.263792    1.256153   -1.392738

21.H        -3.990184    1.769658    0.245799

22.H        -3.596875    1.509515    1.981075

23.H        -3.883674    0.089635    0.919098

24.Mg       -0.773528    0.226053    2.103532

25.F         0.502687    3.287519    5.672223

26.F         1.645700    4.523020    4.249688

27.F         1.940735    2.343691    4.296553

28.F        -1.793287    5.177554    0.684731

29.F        -1.390307    3.652909   -0.848047

30.B        -1.878304   -1.731778    2.502143

31.H        -2.325327   -1.542998    1.374901

32.H        -2.382398   -2.671057    3.063184

33.H        -0.651546   -1.892873    2.422094

34.H        -2.108092   -0.711995    3.196699

35.N         0.291449    2.964803    1.713099

36.S        -0.398354    3.148380    3.149020

37.S         0.755351    4.204612    0.748377

38.C         1.028898    3.341363    4.424694

39.C        -0.860017    4.713478   -0.167377

40.O         1.564979    3.599154   -0.306822

41.O         1.187785    5.409571    1.435229

42.O        -1.263561    4.286385    3.393457

43.O        -0.935820    1.787625    3.463413

44.F        -0.550969    5.678971   -1.064259

Table S2: Mg(BH4)(TFSI)(DGM)-2 + 2 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        557.80 ppm

Atom         X           Y           Z   (Angstrom)

1.O         1.286289    1.244150   -1.118534

2.C         2.719326    1.400587   -1.028635

3.C         3.146954    0.582752    0.182029

4.O         2.361161    1.041460    1.312840

5.C         2.642434    0.270357    2.512636

6.C         0.622590    2.085546   -2.111474

7.C        -0.860946    1.853361   -1.916363

8.O        -1.153439    2.119343   -0.507154

9.C        -2.551458    1.886106   -0.197110

10.H         2.964624    2.462453   -0.897144

11.H         3.196441    1.009281   -1.939857

12.H         4.216067    0.733991    0.392632

13.H         2.937407   -0.485761    0.021811

14.H         2.046246    0.710940    3.312457

15.H         3.712837    0.348238    2.748952

16.H         2.345771   -0.774855    2.353537

17.H         0.914455    1.764808   -3.118171

18.H         0.897875    3.131407   -1.923065

19.H        -1.121141    0.813417   -2.140825

20.H        -1.435945    2.531134   -2.554682

21.H        -3.168808    2.585608   -0.776172

22.H        -2.675369    2.059311    0.874039

23.H        -2.812997    0.846638   -0.438095

24.Mg        0.294827    1.263029    0.756025

25.F        -0.885964    2.725069    6.017950

26.F         0.944405    3.478560    5.050251

27.F         0.403298    1.349985    4.875490

28.F        -0.970924    6.480083    1.553204

29.F        -1.883644    4.705749    0.626725

30.B        -0.296557   -0.954738    1.000361

31.H        -0.951674   -0.479340    0.068418

32.H        -0.806895   -1.967371    1.411523

33.H         0.859892   -1.126305    0.627178

34.H        -0.296862   -0.141896    1.958222

35.N        -0.037228    2.924870    2.132292

36.S        -1.133784    2.997562    3.365433

37.S         0.695661    4.297930    1.577082

38.C        -0.087806    2.618648    4.931342

39.C        -0.733509    5.399070    0.793376

40.O         1.458795    3.835748    0.414722

41.O         1.310455    5.142025    2.583694

42.O        -1.656848    4.337862    3.581877

43.O        -2.005849    1.840816    3.225777

44.F        -0.311349    5.816594   -0.433200

45.C        -1.181068   -0.764726   -4.654452

46.O        -2.359892    4.187634   -3.717659

47.O        -2.232923    1.406973   -4.706041

48.C        -1.618503    0.403536   -5.526813

49.H        -2.341725    0.041527   -6.281240

50.H        -1.010391   -1.652492   -5.291648

51.H        -1.986899   -1.003637   -3.937025

52.H         1.269445   -1.050439   -2.461514

53.H         0.497221   -2.389664   -3.384633

54.H        -0.442594   -1.442633   -2.175335

55.H        -3.368594    2.238749   -6.250176

56.H        -1.786075    3.026358   -5.953378

57.H        -4.077857    3.010686   -3.914076

58.H        -3.876359    4.293065   -5.150264

59.H        -3.573908    5.812536   -3.170724

60.H        -2.155430    5.452450   -2.125537

61.H        -3.612715    4.411973   -2.049348

62.O         0.023209   -0.422718   -3.957597

63.C         0.347421   -1.389444   -2.942017

64.C        -2.653293    2.547324   -5.464783

65.C        -3.339260    3.542046   -4.541749

66.C        -2.965786    5.012690   -2.713159

67.H        -0.744233    0.821357   -6.057335

Table S3: Mg(BH4)(TFSI)(DGM)-2 + 4 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        560.38 ppm

Atom         X           Y           Z   (Angstrom)

1.O         0.418662    1.083719    2.526549

2.C         1.016221    2.404545    2.331488

3.C         0.262056    3.363206    3.230887

4.O        -1.148708    3.181556    2.933358

5.C        -1.987138    4.226272    3.489365

6.C         0.844575    0.120837    1.522462

7.C        -0.041465   -1.104962    1.679177

8.O        -1.411680   -0.633365    1.747030

9.C        -2.378056   -1.720326    1.799787

10.H         0.901664    2.685566    1.279657

11.H         2.081328    2.378379    2.592513

12.H         0.557274    4.390372    2.996904

13.H         0.428001    3.136070    4.296673

14.H        -3.017359    3.946915    3.262525

15.H        -1.729772    5.175683    3.008939

16.H        -1.853531    4.265494    4.579975

17.H         1.898251   -0.147266    1.690438

18.H         0.729683    0.572038    0.531694

19.H         0.187109   -1.676700    2.587989

20.H         0.076636   -1.755745    0.799682

21.H        -2.312893   -2.296771    0.865703

22.H        -3.364192   -1.270198    1.905493

23.H        -2.178206   -2.357968    2.667283

24.Mg       -1.724083    1.186166    2.745992

25.F        -4.216927    4.445743    1.023006

26.F        -3.705243    4.559402   -1.113136

27.F        -2.126047    4.764827    0.402596

28.F        -1.976205    0.289778   -2.768470

29.F        -0.193862   -0.366145   -1.652587

30.B        -2.674923    0.812190    4.787097

31.H        -3.050216    0.126242    3.821673

32.H        -2.997735    0.235634    5.797641

33.H        -1.430540    0.897124    4.755586

34.H        -3.154149    1.931783    4.681872

35.N        -1.427244    1.985439   -0.125138

36.S        -3.009469    2.208637    0.069453

37.S        -0.641793    2.304506   -1.514040

38.C        -3.272304    4.140687    0.090336

39.C        -0.713080    0.624569   -2.438716

40.O         0.775545    2.434553   -1.179512

41.O        -1.288210    3.266711   -2.395746

42.O        -3.930782    1.698838   -0.930205

43.O        -3.252062    1.803119    1.485586

44.F         0.033322    0.707248   -3.567963

45.C         2.647050    5.848832    0.948418

46.H         1.055890    6.196959   -0.458796

47.H         1.038758    4.576170    0.271679

48.H         2.767605    6.863776    1.361785

49.H         3.339407    5.722830    0.095527

50.C        -1.049716    7.795262    2.490518

51.H         5.043014    5.086794    1.809224

52.H         4.405532    4.365419    3.323071

53.H         4.248877    6.133327    3.036554

54.O        -2.340271    7.325627    2.053769

55.C         1.208974    5.637797    0.480305

56.C         4.236701    5.136867    2.562418

57.H        -0.344647    7.766240    0.452361

58.C        -3.332010    7.503562    3.062676

59.O         2.960070    4.875124    1.968326

60.O         0.243203    6.037428    1.462624

61.C         0.000662    7.460630    1.451708

62.H         0.910709    8.018753    1.705505

63.H        -1.065929    8.884411    2.640082

64.H        -0.782426    7.318821    3.451534

65.H        -4.275582    7.115929    2.663170

66.H        -3.452109    8.570974    3.327717

67.H        -3.069352    6.945997    3.981458

68.C        -5.462004   -3.104098    4.088625

69.H        -4.851829   -5.179689    4.197033

70.H        -4.370013   -4.335710    2.690878

71.H        -5.321121   -2.777006    5.134073

72.H        -6.496937   -3.479979    3.975502

73.C        -0.885677   -4.466285    4.754179

74.H        -6.932217   -0.909293    3.722496

75.H        -5.611640   -0.036310    2.871133

76.H        -5.409047   -0.475918    4.591701

77.O        -0.286280   -3.219267    4.378613

78.C        -4.476178   -4.224623    3.785044

79.C        -5.837206   -0.794422    3.628039

80.H        -1.993047   -4.735807    2.905835

81.C        -0.820713   -2.074094    5.090469

82.O        -5.230331   -2.019026    3.185291

83.O        -3.211164   -3.904232    4.382677

84.C        -2.170312   -4.804540    3.995255

85.H        -2.453855   -5.850010    4.232128

86.H        -0.146884   -5.247548    4.524065

87.H        -1.091485   -4.482427    5.838840

88.H        -0.207294   -1.214401    4.803863

89.H        -0.741733   -2.231196    6.179246

90.H        -1.866486   -1.878350    4.830995

91.C         2.181665    9.021230    4.638697

92.H         2.418774   11.142732    4.338403

93.H         2.998737   10.134980    2.973460

94.H         1.254863    9.037222    5.240002

95.H         3.045449    9.056015    5.329098

96.C        -0.489043   11.414003    1.466381

97.H         2.566371    6.492688    5.421835

98.H         1.915731    5.824493    3.879776

99.H         0.846372    6.757809    4.980359

100.O        -0.454526   10.388214    0.471202

101.C         2.202373   10.242892    3.731746

102.C         1.870762    6.661826    4.579507

103.H         1.670016   11.400680    1.442930

104.C        -1.758905   10.096420   -0.050537

105.O         2.233283    7.834120    3.838151

106.O         0.924408   10.363047    3.100205

107.C         0.852869   11.462034    2.183353

108.H         0.945311   12.419475    2.729676

109.H        -0.694231   12.395430    0.998414

110.H        -1.285813   11.210755    2.206028

111.H        -1.627420    9.343454   -0.834192

112.H        -2.225889   10.999507   -0.482376

113.H        -2.411505    9.680334    0.735238

Table S3: Mg(BH4)(TFSI)(DGM)-2 + 6 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        561.87 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -0.839366    1.710146    3.736717

2.C         0.301877    2.596839    3.584349

3.C         0.083783    3.774475    4.523488

4.O        -1.281574    4.229840    4.321602

5.C        -1.575196    5.481820    4.999865

6.C        -0.891283    0.677905    2.702708

7.C        -2.273223    0.047284    2.742186

8.O        -3.244053    1.120559    2.866941

9.C        -4.612276    0.709907    2.581040

10.H         0.354356    2.932548    2.544139

11.H         1.224686    2.059035    3.837577

12.H         0.782500    4.582717    4.268732

13.H         0.203902    3.482631    5.578935

14.H        -2.631099    5.688181    4.811471

15.H        -0.944199    6.274374    4.579780

16.H        -1.411479    5.361898    6.080552

17.H        -0.118907   -0.062122    2.919174

18.H        -0.695374    1.155733    1.738223

19.H        -2.378504   -0.635864    3.589761

20.H        -2.465574   -0.489850    1.807890

21.H        -4.695592    0.456766    1.519278

22.H        -5.237379    1.567628    2.831668

23.H        -4.890003   -0.151216    3.195210

24.Mg       -2.672326    2.659059    4.121464

25.F        -4.556181    6.613715    2.083771

26.F        -3.374434    6.571935    0.230324

27.F        -2.355736    6.540331    2.182250

28.F        -3.254643    2.386684   -1.610168

29.F        -2.223656    0.999510   -0.240296

30.B        -3.621801    2.344144    6.161648

31.H        -4.390193    2.122212    5.213230

32.H        -4.119569    1.946788    7.187584

33.H        -2.562772    1.722255    5.962576

34.H        -3.371546    3.549097    6.199777

35.N        -2.068613    3.612959    1.313555

36.S        -3.542518    4.185912    1.531787

37.S        -1.293222    3.554269   -0.114005

38.C        -3.439128    6.111508    1.495005

39.C        -2.068989    2.062994   -1.064535

40.O         0.059687    3.085955    0.177612

41.O        -1.496952    4.711273   -0.977407

42.O        -4.578619    3.844570    0.567914

43.O        -3.841066    3.945147    2.970243

44.F        -1.211519    1.709566   -2.062233

45.C         1.923937    5.577754    1.154865

46.H        -0.069290    6.327897    0.910253

47.H         0.069476    5.031643    2.112176

48.H         2.504400    6.492258    0.955120

49.H         1.790240    5.012993    0.217665

50.C         0.856068    9.169054    3.525330

51.H         4.006027    3.995309    0.713714

52.H         4.471150    3.913468    2.443011

53.H         4.526162    5.485926    1.570936

54.O        -0.422742    9.295634    4.181341

55.C         0.555658    5.930042    1.725921

56.C         3.984444    4.531241    1.679704

57.H        -0.124758    8.491323    1.730268

58.C        -0.353939   10.227270    5.256863

59.O         2.639628    4.757751    2.110145

60.O         0.617799    6.865572    2.815820

61.C         0.748774    8.225930    2.347098

62.H         1.659546    8.345228    1.746216

63.H         1.190482   10.147937    3.148587

64.H         1.607339    8.791364    4.241828

65.H        -1.350155   10.282211    5.710713

66.H        -0.060325   11.233125    4.896904

67.H         0.379631    9.908268    6.021354

68.C        -8.338427   -0.785962    2.940788

69.H        -8.439171   -2.942192    3.040708

70.H        -7.314916   -2.300355    1.804164

71.H        -8.428651   -0.505659    4.005565

72.H        -9.353904   -0.823171    2.502389

73.C        -4.694912   -3.531467    4.576030

74.H        -9.006512    1.668459    2.140472

75.H        -7.299827    2.168086    1.891911

76.H        -7.884730    1.773428    3.540859

77.O        -3.727414   -2.475803    4.653491

78.C        -7.687869   -2.157415    2.832324

79.C        -7.962975    1.517316    2.470638

80.H        -5.243508   -3.171877    2.506649

81.C        -4.143190   -1.382602    5.511459

82.O        -7.536465    0.170081    2.235822

83.O        -6.610213   -2.255346    3.773461

84.C        -5.738201   -3.356244    3.472106

85.H        -6.320830   -4.297804    3.405581

86.H        -4.135739   -4.451858    4.348946

87.H        -5.201450   -3.662211    5.548321

88.H        -3.350824   -0.632625    5.482024

89.H        -4.266463   -1.744058    6.546658

90.H        -5.087004   -0.944479    5.168157

91.C         4.858059    9.203868    2.307482

92.H         5.206874   10.848630    0.952045

93.H         4.282659    9.485718    0.242443

94.H         4.767335    9.770375    3.251520

95.H         5.918308    8.915880    2.174489

96.C         1.295695   12.070429    0.889925

97.H         5.071288    6.959485    3.809108

98.H         3.334834    6.547187    3.542667

99.H         3.782860    8.050346    4.421393

100.O         0.331187   11.015445    0.875191

101.C         4.421121   10.095387    1.153360

102.C         4.061909    7.361749    3.605185

103.H         2.512443   10.899753   -0.456837

104.C        -0.884974   11.385840    1.534497

105.O         4.024561    8.040870    2.342125

106.O         3.195144   10.739870    1.513876

107.C         2.643599   11.520747    0.447028

108.H         3.319554   12.361482    0.199811

109.H         0.986464   12.885565    0.208045

110.H         1.394621   12.490245    1.908508

111.H        -1.553956   10.521912    1.482224

112.H        -1.355597   12.256249    1.042381

113.H        -0.697614   11.625490    2.595577

114.C        -2.981934   -3.101291    1.103958

115.C        -4.602915   -2.286602   -0.498726

116.C        -6.133635    1.063388   -0.907146

117.H        -3.328722   -4.116601    0.837919

118.C        -0.448279   -2.766537   -1.597345

119.O        -5.122971    0.044466   -0.836217

120.O        -3.983678   -2.126360    0.795693

121.H        -2.849228   -3.042560    2.192409

122.H        -0.858220   -3.442154    0.961090

123.H        -1.367642   -1.775058    0.570012

124.H        -0.536514   -3.047309   -2.652047

125.H         0.428742   -3.273505   -1.154147

126.H        -0.305455   -1.674683   -1.515508

127.C        -5.703314   -1.249408   -0.645051

128.H        -5.046596   -3.297778   -0.568315

129.H        -3.859799   -2.175636   -1.299552

130.H        -6.343197   -1.242140    0.253453

131.H        -6.329145   -1.520829   -1.518579

132.C        -1.629605   -2.839361    0.446302

133.H        -6.762497    0.925829   -1.806442

134.H        -5.618945    2.025842   -0.952662

135.H        -6.777533    1.028486   -0.014654

136.O        -1.659307   -3.173236   -0.946838

137.C         1.578580   -1.975896    1.933370

138.C         0.002053   -2.654381    3.594746

139.C        -0.983062   -0.930840    6.717559

140.H         0.700472   -1.762929    1.305468

141.C         2.919669    1.436305    1.395615

142.O        -0.710433   -1.153079    5.330389

143.O         1.221992   -1.949957    3.321196

144.H         1.968291   -2.973806    1.656417

145.H         3.095420   -1.112040    0.671317

146.H         3.428805   -0.964333    2.428436

147.H         2.343805    2.364835    1.419481

148.H         3.390092    1.314717    0.402883

149.H         3.716560    1.476025    2.160216

150.C        -0.352794   -2.510249    5.066099

151.H         0.113445   -3.728400    3.352796

152.H        -0.816950   -2.247322    2.982276

153.H         0.510579   -2.811146    5.688597

154.H        -1.209105   -3.173945    5.286902

155.C         2.636027   -0.915349    1.659504

156.H        -1.778809   -1.607317    7.076213

157.H        -1.324450    0.104931    6.813125

158.H        -0.075195   -1.093042    7.326335

159.O         2.006690    0.368265    1.662999

Table S3: Mg(BH4)(TFSI)(DGM)-3

NMR Shielding ADF-GUI atom  Mg(24):        569.76 ppm

Atom         X           Y           Z   (Angstrom)

1.O        -0.429487    0.264915   -0.253581

2.C         0.761106    0.645144   -0.984271

3.C         1.927073    0.376876   -0.040225

4.O         1.691765    1.126883    1.178947

5.C         2.667548    0.826779    2.213155

6.C        -1.692745    0.596722   -0.879117

7.C        -2.757061    0.242444    0.150554

8.O        -2.462057    0.983532    1.364222

9.C        -3.363557    0.616704    2.447408

10.H         0.704175    1.707380   -1.253293

11.H         0.859971    0.027639   -1.889085

12.H         2.870745    0.709237   -0.496937

13.H         1.977775   -0.694030    0.206786

14.H         2.403795    1.449146    3.071787

15.H         3.671749    1.084838    1.851253

16.H         2.601297   -0.235893    2.481808

17.H        -1.832681   -0.004260   -1.789673

18.H        -1.710221    1.668012   -1.122693

19.H        -2.721538   -0.832582    0.381978

20.H        -3.755063    0.523318   -0.217910

21.H        -4.390151    0.886672    2.163632

22.H        -3.050964    1.186038    3.323334

23.H        -3.267621   -0.456834    2.650420

24.Mg       -0.365099    1.037565    1.769954

25.F        -2.627262    3.160363    4.844854

26.F        -2.918830    3.721740    2.732805

27.F        -2.583354    5.281716    4.252904

28.F         2.506819    3.813250    1.634307

29.F         2.319500    5.658018    0.456704

30.B        -0.445823   -1.129932    2.826929

31.H        -1.402658   -1.573974    2.209653

32.H        -0.055004   -1.855640    3.713767

33.H         0.480811   -0.929620    2.034209

34.H        -0.781789   -0.056443    3.369121

35.N        -0.165608    4.862358    2.321625

36.S        -0.365284    3.891070    3.578349

37.S        -0.023869    4.363402    0.806314

38.C        -2.253234    4.033459    3.875848

39.C         1.884588    4.389182    0.577848

40.O        -0.522015    5.350072   -0.130238

41.O        -0.405869    2.952386    0.573936

42.O        -0.191978    2.436745    3.304028

43.O         0.267168    4.416476    4.768544

44.F         2.213084    3.701473   -0.552910

Table S3: Mg(BH4)(TFSI)(DGM)-3 + 2 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        568.02 ppm

Atom         X           Y           Z   (Angstrom)

1.O         1.753789   -0.187764    2.869543

2.C         2.981691    0.344612    2.331050

3.C         3.357554    1.510342    3.238513

4.O         2.235264    2.428947    3.266225

5.C         2.418433    3.499506    4.230850

6.C         1.085114   -1.206664    2.073174

7.C        -0.234619   -1.463972    2.773263

8.O        -0.938704   -0.181401    2.846551

9.C        -2.213558   -0.315349    3.540332

10.H         2.819851    0.681058    1.298958

11.H         3.771907   -0.420773    2.359319

12.H         4.245177    2.030975    2.849940

13.H         3.545534    1.149277    4.260816

14.H         1.530530    4.132099    4.159989

15.H         3.317007    4.074775    3.969834

16.H         2.497472    3.074551    5.240427

17.H         1.692988   -2.122582    2.055256

18.H         0.933725   -0.830654    1.053391

19.H        -0.070917   -1.826599    3.794809

20.H        -0.847558   -2.171137    2.207899

21.H        -2.813883   -1.076546    3.030026

22.H        -2.693673    0.664066    3.495319

23.H        -2.027424   -0.591815    4.583152

24.Mg        0.359122    1.378326    3.375591

25.F        -3.691227    3.235084    3.157930

26.F        -3.054863    2.017883    1.433108

27.F        -3.878808    4.037640    1.115349

28.F         1.938023    4.552642    1.359718

29.F         1.968392    4.639655   -0.835278

30.B         0.191536    0.916601    5.745606

31.H        -0.054275   -0.278797    5.760818

32.H         0.204269    1.433937    6.842129

33.H         1.301868    1.083927    5.222121

34.H        -0.687027    1.494013    5.078642

35.N        -0.818239    3.824540    0.584353

36.S        -1.358179    4.013492    2.081398

37.S         0.291430    2.757227    0.146114

38.C        -3.119618    3.282626    1.931559

39.C         1.900436    3.812347    0.226309

40.O         0.149508    2.400599   -1.253009

41.O         0.526861    1.658224    1.103887

42.O        -0.731148    3.140522    3.109322

43.O        -1.541525    5.408252    2.423968

44.F         2.984955    2.986221    0.208183

45.C        -2.839313   -2.435554   -0.223610

46.H        -3.785451   -4.301574    0.304426

47.H        -1.996434   -4.320345    0.405944

48.H        -3.602428   -1.727795    0.147648

49.H        -3.070205   -2.671712   -1.279442

50.C        -3.019711   -4.095426    4.294660

51.H        -1.755185   -0.569166   -1.765599

52.H        -0.455643   -0.182242   -0.594573

53.H        -2.157949    0.141783   -0.164334

54.O        -1.831035   -3.406115    4.687013

55.C        -2.897870   -3.712402    0.600268

56.C        -1.480471   -0.545004   -0.696877

57.H        -1.946447   -5.052804    2.680776

58.C        -1.924285   -2.884076    6.020471

59.O        -1.532236   -1.861024   -0.120926

60.O        -2.979077   -3.371899    1.992088

61.C        -2.903583   -4.525224    2.840443

62.H        -3.729290   -5.223051    2.607035

63.H        -3.169726   -4.994698    4.922298

64.H        -3.900922   -3.438646    4.415769

65.H        -1.023503   -2.288097    6.199107

66.H        -1.997752   -3.700583    6.760417

67.H        -2.808180   -2.230346    6.123666

Table S3: Mg(BH4)(TFSI)(DGM)-3 + 4 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        569.77 ppm

1.O         3.563435   -0.363763    3.205171

2.C         4.830835    0.032577    2.629305

3.C         5.527000    0.839848    3.716406

4.O         4.622835    1.902400    4.137257

5.C         5.143138    2.659115    5.259167

6.C         2.655031   -1.060463    2.313224

7.C         1.385996   -1.264650    3.123212

8.O         0.955267    0.040843    3.613396

9.C        -0.168753   -0.064163    4.525737

10.H         4.648593    0.637793    1.732852

11.H         5.408567   -0.860155    2.365930

12.H         6.454437    1.288412    3.330546

13.H         5.739281    0.205298    4.588650

14.H         4.399235    3.426929    5.487684

15.H         6.094121    3.128478    4.971208

16.H         5.272182    1.992253    6.121967

17.H         3.096380   -2.020575    2.027312

18.H         2.477991   -0.447075    1.425436

19.H         1.581195   -1.912218    3.989425

20.H         0.591741   -1.690950    2.494098

21.H        -1.029100   -0.492083    3.992691

22.H        -0.399953    0.949921    4.857507

23.H         0.116020   -0.684440    5.385956

24.Mg        2.618175    1.202027    4.236690

25.F        -1.411315    3.257934    4.543303

26.F        -0.681217    2.496001    2.604213

27.F        -1.415714    4.568692    2.771943

28.F         4.568757    4.474342    2.740389

29.F         4.227590    5.193529    0.690870

30.B         2.897850    0.084710    6.406694

31.H         2.331534   -0.803547    5.780801

32.H         2.779586   -0.059743    7.603987

33.H         4.072461    0.136893    6.065781

34.H         2.346431    1.182352    6.156554

35.N         1.637504    4.456489    2.389413

36.S         1.019520    4.165165    3.832550

37.S         2.416063    3.367537    1.505323

38.C        -0.749529    3.587250    3.401979

39.C         4.181002    4.123921    1.487118

40.O         2.001875    3.374860    0.117115

41.O         2.579651    2.042201    2.143065

42.O         1.589565    2.998643    4.561563

43.O         0.870162    5.399062    4.578667

44.F         5.049972    3.175148    1.020117

45.C        -0.316817    1.504043   -1.620833

46.H        -0.861659    2.849048   -3.200135

47.H        -2.265430    2.121877   -2.351755

48.H         0.605652    2.009275   -1.299376

49.H        -0.061490    0.758924   -2.400328

50.C        -1.762326    6.016590   -1.029468

51.H         0.512226   -0.651782   -0.287264

52.H        -0.544991   -0.303724    1.123455

53.H         0.771652    0.824781    0.697626

54.O        -2.640031    5.979215    0.102686

55.C        -1.255414    2.546740   -2.209404

56.C         0.007531    0.145569    0.291529

57.H        -3.055796    4.584174   -2.023153

58.C        -2.303246    7.008131    1.038089

59.O        -0.943126    0.854637   -0.506603

60.O        -1.295079    3.677424   -1.337396

61.C        -1.977457    4.796195   -1.911865

62.H        -1.559164    5.011128   -2.914517

63.H        -1.959852    6.931125   -1.624332

64.H        -0.711339    6.031666   -0.702275

65.H        -2.996713    6.920824    1.881077

66.H        -2.406251    8.011202    0.580989

67.H        -1.267663    6.891352    1.399913

68.C         1.472165    7.881995    1.056262

69.H         0.247515    8.224427   -0.678696

70.H         1.970076    8.676136   -0.895134

71.H         0.999696    6.967166    1.453378

72.H         0.970599    8.761424    1.506697

73.C         1.348517    5.106249   -2.845179

74.H         2.644325    8.608438    3.338375

75.H         4.167657    7.743656    2.940458

76.H         2.637620    6.825606    3.162444

77.O         2.715458    4.697314   -3.009343

78.C         1.289730    7.926012   -0.453704

79.C         3.083275    7.758007    2.783159

80.H         2.025131    7.165270   -2.961930

81.C         2.813027    3.283080   -3.172410

82.O         2.868167    7.897819    1.373702

83.O         1.545052    6.627644   -0.995267

84.C         1.290684    6.560243   -2.400769

85.H         0.279130    6.954559   -2.616971

86.H         0.812469    4.999335   -3.809825

87.H         0.843444    4.486560   -2.088957

88.H         3.875869    3.042980   -3.292603

89.H         2.261166    2.940545   -4.070359

90.H         2.415086    2.757825   -2.291124

91.C         5.838569   -3.770399    2.881232

92.H         6.285212   -4.613863    0.946115

93.H         4.535302   -4.475498    1.308538

94.H         6.748421   -3.147633    2.974243

95.H         6.046171   -4.753259    3.345667

96.C         4.933293   -1.382133   -1.190461

97.H         5.216386   -3.588742    5.509510

98.H         4.174639   -2.138812    5.225114

99.H         5.926799   -2.070364    4.873567

100.O         3.756349   -0.769277   -0.654375

101.C         5.513027   -3.971415    1.408648

102.C         5.029485   -2.715341    4.860205

103.H         4.122916   -3.320905   -0.701128

104.C         3.576989    0.568722   -1.140774

105.O         4.732068   -3.130463    3.516671

106.O         5.476552   -2.691694    0.761754

107.C         5.083041   -2.781780   -0.613414

108.H         5.846389   -3.333578   -1.193271

109.H         4.858109   -1.455587   -2.292007

110.H         5.826941   -0.779459   -0.944886

111.H         2.667708    0.963344   -0.682238

112.H         3.470466    0.579582   -2.239010

113.H         4.428470    1.212161   -0.861994

Table S3. Mg(BH4)(TFSI)(DGM)-3 + 6 DGMs

NMR Shielding ADF-GUI atom  Mg(24):        567.73 ppm

1.O         1.952442    1.824690   -2.292106

2.C         1.340961    2.689803   -3.282873

3.C         2.515218    3.333745   -4.000396

4.O         3.407068    3.911807   -3.000470

5.C         4.620626    4.441827   -3.589402

6.C         1.030537    1.075258   -1.448845

7.C         1.896951    0.409037   -0.398770

8.O         2.699329    1.468602    0.240507

9.C         3.655771    0.927719    1.191025

10.H         0.705349    3.427160   -2.779453

11.H         0.743320    2.094850   -3.979998

12.H         2.170336    4.130006   -4.676734

13.H         3.077833    2.576816   -4.567147

14.H         5.218960    4.845974   -2.771210

15.H         4.357783    5.235738   -4.303284

16.H         5.179574    3.632271   -4.075777

17.H         0.509690    0.317705   -2.042462

18.H         0.298740    1.765216   -1.017900

19.H         2.582960   -0.314456   -0.856009

20.H         1.285994   -0.093572    0.355904

21.H         3.111131    0.493714    2.037044

22.H         4.275112    1.763866    1.521247

23.H         4.271526    0.162156    0.708581

24.Mg        3.458712    2.812396   -1.176863

25.F         4.897335    3.625663    3.196319

26.F         2.717128    3.523590    2.895900

27.F         3.614939    5.270957    3.900222

28.F         3.478605    6.544232   -1.737957

29.F         1.860642    7.963775   -1.286035

30.B         5.594718    1.734488   -1.777028

31.H         4.498868    1.166097   -1.687969

32.H         6.368893    1.169006   -1.028520

33.H         5.940316    1.703551   -2.947067

34.H         5.510984    2.919054   -1.435006

35.N         2.573505    5.924386    1.062476

36.S         4.011148    5.218901    1.232578

37.S         1.551216    5.550677   -0.113580

38.C         3.790200    4.357078    2.921624

39.C         2.140369    6.670275   -1.555924

40.O         0.225111    6.052279    0.202178

41.O         1.665049    4.181410   -0.646778

42.O         4.274977    4.085193    0.315933

43.O         5.073540    6.180794    1.442318

44.F         1.503139    6.316223   -2.702238

45.C         2.952076   -2.347865    2.464543

46.H         4.358590   -3.727460    1.627511

47.H         2.732810   -3.809070    0.880412

48.H         3.673881   -1.566629    2.763152

49.H         2.833558   -3.049653    3.312819

50.C         5.018057   -1.929209   -1.908319

51.H         0.998220   -1.700863    4.121394

52.H         0.164690   -0.638895    2.954014

53.H         1.798417   -0.204550    3.552360

54.O         3.840750   -1.613990   -2.662816

55.C         3.503271   -3.120660    1.273386

56.C         1.136326   -1.034554    3.253183

57.H         4.022840   -3.711824   -1.212754

58.C         4.135340   -0.842409   -3.840017

59.O         1.688587   -1.759926    2.142133

60.O         3.931076   -2.220275    0.248581

61.C         4.646890   -2.900410   -0.796828

62.H         5.569786   -3.346110   -0.381054

63.H         5.761476   -2.427781   -2.560567

64.H         5.471849   -1.010754   -1.501104

65.H         3.170565   -0.565715   -4.273739

66.H         4.712715   -1.451515   -4.562026

67.H         4.704601    0.061353   -3.587263

68.C        -3.573504    4.883400    1.812788

69.H        -2.226249    6.371505    1.014269

70.H        -3.220388    6.932039    2.401494

71.H        -2.965304    3.972701    1.688328

72.H        -4.195977    5.025293    0.908324

73.C         0.476103    6.176713    3.956728

74.H        -5.720421    3.376443    2.067406

75.H        -5.774783    3.521473    3.856341

76.H        -4.405472    2.671923    3.059715

77.O         0.061158    5.662954    5.233710

78.C        -2.650508    6.079009    1.991190

79.C        -5.113030    3.514431    2.982728

80.H        -1.246732    7.493843    3.886294

81.C         1.090512    4.891985    5.855943

82.O        -4.420622    4.762174    2.967855

83.O        -1.600041    5.696369    2.881275

84.C        -0.723005    6.770602    3.236126

85.H        -0.364668    7.288529    2.331349

86.H         1.254400    6.949479    4.087705

87.H         0.896836    5.368217    3.338831

88.H         0.693628    4.544240    6.816533

89.H         1.999134    5.495238    6.030678

90.H         1.363163    4.021498    5.233720

91.C        -0.869913    2.627397    3.824125

92.H        -1.686802    2.163318    5.769719

93.H        -2.809036    1.899084    4.399248

94.H         0.187379    2.351564    3.997634

95.H        -1.001642    3.695445    4.049456

96.C        -1.797013   -1.897918    5.123064

97.H        -0.276149    4.046596    1.706916

98.H        -0.743563    2.784361    0.531164

99.H         0.670880    2.520175    1.592421

100.O        -1.873701   -2.300401    3.750482

101.C        -1.760717    1.797904    4.729782

102.C        -0.334830    2.965569    1.529219

103.H        -3.282174   -0.365720    4.778730

104.C        -1.305212   -3.595344    3.545116

105.O        -1.235189    2.349770    2.463373

106.O        -1.350908    0.418152    4.662294

107.C        -2.294385   -0.467381    5.264221

108.H        -2.413846   -0.238542    6.340967

109.H        -2.419194   -2.564308    5.750072

110.H        -0.752603   -1.960122    5.480101

111.H        -1.422468   -3.831371    2.483050

112.H        -1.819622   -4.359761    4.155279

113.H        -0.230161   -3.598111    3.800916

114.C        -1.857267   -0.291139    0.887948

115.H        -0.679906   -1.978895    1.416270

116.H        -2.178593   -2.393877    0.535859

117.H        -1.087905    0.461895    0.658477

118.H        -2.070897   -0.229488    1.965809

119.C         1.061979   -2.949494   -1.933675

120.H        -3.888866    1.148516    1.655247

121.H        -4.599837    1.312512    0.014751

122.H        -3.010927    2.060749    0.401210

123.O         0.345164   -3.210945   -3.154667

124.C        -1.336759   -1.680782    0.588256

125.C        -3.666195    1.193645    0.577317

126.H        -0.604161   -3.795305   -0.849349

127.C         1.225840   -3.162938   -4.284681

128.O        -3.057281   -0.021933    0.132793

129.O        -0.581684   -1.711252   -0.639794

130.C         0.116537   -2.962675   -0.749628

131.H         0.712549   -3.116964    0.165643

132.H         1.828652   -3.733555   -1.786991

133.H         1.592310   -1.989328   -1.988682

134.H         0.629382   -3.430899   -5.164702

135.H         2.056004   -3.882893   -4.170281

136.H         1.652460   -2.156872   -4.415488

137.C        -0.113508   -0.329417   -5.693959

138.H        -1.842772   -1.061426   -4.669666

139.H        -0.395962   -0.980942   -3.644045

140.H        -0.623234    0.330896   -6.418536

141.H         0.003235   -1.329606   -6.147040

142.C        -2.751018    2.158348   -2.521580

143.H         2.148330   -0.559776   -7.070655

144.H         2.952065    0.789334   -6.205015

145.H         1.516060    1.111416   -7.237283

146.O        -1.757171    2.880197   -1.773173

147.C        -0.950286   -0.452027   -4.433022

148.C         1.985914    0.395613   -6.539403

149.H        -1.765561    0.295846   -2.011036

150.C        -2.214214    4.196764   -1.441142

151.O         1.182274    0.208389   -5.373422

152.O        -1.353011    0.855262   -3.999577

153.C        -2.251841    0.769398   -2.874394

154.H        -3.122178    0.145732   -3.147920

155.H        -3.666836    2.065134   -1.915285

156.H        -2.997259    2.711074   -3.446700

157.H        -1.442914    4.668688   -0.828522

158.H        -3.156985    4.150341   -0.869545

159.H        -2.384728    4.796428   -2.353041